## Slide 1: Nanoplasmonics: Correlated LSPR and TEM Emilie Ringe, Yingmin Wang, R. Van Duyne & L. D. Marks
Collaborators:
Theory: G.C. Schatz
Synthesis: J. Huang, C. Mirkin , +++
Materials Research Science & Engineering Center
Northwestern University

## Slide 2: Localized Surface Plasmon Resonance (LSPR)
Small particles of noble metal: used in stained glass since the middle ages
Wide range of colors depending on shape and size
L. Liz-Marzan, Mater. Today 7, 21 (2004)
Kings’ College, Cambridge
Notes: 2

## Slide 3: Synthesis yields Particles with Heterogeneous Optical Properties
10 μm
10 μm
Hollow-Cone DF = ADF

## Slide 4: Gold Octahedra: Ensemble versus Single Particle
SINGLE PART.
Slope=1.69(0.03)
ENSEMBLE
Slope ~1.1
C. Li, et al., ACS Nano. 2, 1760 (2008)

## Slide 5: Follow the science, not the electron
For real commercial applications, we need five-sigma reliability
The £64,000 questions:
  How, in detail, do the plasmonic properties depend upon the size/shape/environment?
  How, in detail, do we control the shape/size with 100% reliability (chemical potential, growth/thermodynamics…)?

## Slide 6: Strategy
Growth
Thermodynamic
Kinetic
Modified Kinetic Wulff shapes for Twinned Nanoparticles. Ringe, E., R.P. Van Duyne, and L.D. Marks, JPC C, 2013. 117: p. 15859.
Thermodynamic Analysis of Multiply Twinned Particles: Surface Stress Effects. Patala, S., L.D. Marks, and M. Olvera de la Cruz, JPCL, 2013. 4: p. 3089.
Elastic Strain Energy Effects in Faceted Decahedral Nanoparticles. Patala, S., L.D. Marks, and M.O. de la Cruz, JPC C, 2013. 117(3): p. 1485.
Correlated measurements tools

## Slide 7: Goal: Build the Nanoplasmonics Toolbox
10 μm

## Slide 8: Three parts to talk today
How to combine TEM & LSPR
Follow the science, not the electron
Thousands of nanoparticles
A picture is worth a thousand words, but numbers are worth thousands of pictures
A few grey-haired thoughts

## Slide 9: How to find the needle in a haystack….fast
Target
  Measure the optical response of nanoparticles, both single and (serendipity) small clusters of nanoparticles
  Determine the structure of exactly the same particles by TEM
  Close the loop with theoretical calculations
Y. Wang et al, Ultramicroscopy 2009, 109, 1110-1113.

## Slide 10: Method
(1,1)
(-2,1)
(-1,1)
(1,2)
(-1,2)
(-2,2)
X
Y
Solvent + Nanoparticles

## Slide 11: Correlated LSPR & TEM Imaging
Low resolution TEM image
LSPR image with 100x objective

## Slide 12: Caveat: Damage I
Structural changes (quasimelting, enhanced surface diffusion etc)
  Patience is a virtue, turn the beam down!
Does the electron beam change the LSPR?
  Yes for TEM, no for SEM (with care)
  Local dielectric environment probably changes
  We always do the LSPR first

## Slide 13: Caveat: Damage II
Optical damage?
  Possible, with high fluxes, e.g. photoemission expts, but rare
Before After nx1 (111) (not the same nanoparticle) reconstruction
Rounded
A. Grubisic et al, Nano Letters 2012, 12, 4823.

## Slide 14: Narrow: LTP Rods
 = 0.156 eV

633.6 nm

 = 0.120 eV
628.5 nm
Wide Linewidth Defective Particles (Odd ones, rough surfaces?)
FWHM
0.2505 eV
FWHM
0.275 eV
Narrow Linewidth Decagonal Rods

## Slide 15: First Application: Single Silver Nanocube LSPR/TEM/FDTD
Step 1: LSPR
Step 2: TEM
Y. Wang et al, Ultramicroscopy 2009, 109, 1110-1113.
Notes: 15

## Slide 16: FDTD Results: Effect of Size and Corner Rounding in Ag Cubes
J. M. McMahon, et al, JPCC, 113, 2731 (2009)
Effect of size
Effect of corner rounding
Notes: 16

## Slide 17: Reasonable agreement
17
FDTD
L. J. Sherry, et al, Nano Lett., 5, 2034 (2005); J. M. McMahon, et al, JPCC, 113, 2731 (2009)
40 nm
(1) Distal peak, quadrupolar:
Sharp, high energy, EF away from substrate
(2) Proximal peak, dipolar:
Broader, EF extends into the substrate
1
2
Oleic Acid Surfactant
Notes: 17

## Slide 18: Hundreds (thousands) of needles
Measure many nanoparticles
Analyze the results statistically – new details appear
10 μm
10 μm
A picture is worth a thousand words, but numbers are worth a thousand pictures
And thousands of numbers…

## Slide 19: Statistics
183 cubes  5 Trends:
LSPR Redshift with
Size Increase
Ag  Au
Substrate
Ag more sensitive to
Substrate
Size
LSPR TEM
ηSi3N4 ~ 2.05
ηFormvar = 1.5
E. Ringe, et al, JPCC, 114, 12511 (2010)
Ag
Au

## Slide 20: Effect of Size and Substrate, Ag Nanocubes
Proximal
Distal
0.23 eV
Proximal
0.05 eV
Distal
Distal peak  Slope = -4.2(0.55) meV/nm
Proximal peak  Slope = -8.9 (0.5) meV/nm
E. Ringe, et al, JPCC, 114, 12511 (2010)
Notes: 20

## Slide 21: Silver Right Bipyramids
500 nm
Plasmon-mediated synthesis
  Start with “monotwins” seeds
  Control final size w/light 
Size: edge length of triangular base
Rounding: height of triangle removed from corners
See effect of rounding and size on LSPR

## Slide 22: LSPR Dependence on Size and Rounding in Bipyramids
Both Factors play a roleneither accounts for all the variation
R2=75%
R2=49%

## Slide 23: Bipyramids: Fit to Two Parameters and Their Interplay
R2=88%
Ringe et al, Nanotechnology 2012, 23, 444005.

## Slide 24: Correlating the Size, Shape, and Plasmon Energy (Retardation)
Ag cubes 50-200 nm
Ag and Au cubes
on different substrates
Au Icosahedra Au decahedra Au truncated bitetrahedra
Notes: 24

## Slide 25: Experimental Data for Au Particles (Retardation)
If I can't calculate it, I don't understand it Richard Feynman ( & AH?)

## Slide 26
Cubes and rods
Electrons oscillate from one face to another face which is parallel.
Plasmon length=1* edge length
Triangles
Electrons oscillate approx. from an edge to an apex in the plane of the triangular base
Plasmon length=0.866*edge length
J. Nelaya et al. Nano Lett. 10, 902 (2010)
I. Pastoriza-Santos et al., Adv. Funct. Mater.
17, 1443 (2007)
Decahedra (pentagonal bipyramids)
Electrons oscillate approx. from an edge to an apex in the plane of the pentagonal base
Distance travelled=1.306*edge length
Octahedra
In-plane and out-of plane contribute
Distance travelled=1*edge length up to
1.414*edge length
Edge length
Edge length
Edge length
Edge length
C. Li et al., ACS Nano. 2, 1760 (2008)

## Slide 27: Shape Independent Result
Slope = -2.4(6) meV/nm
Slope = -3.02(5)
Slope = -3.3(2)
Slope = -3.22(9)
Slope = -3.06(4)
Plasmon Length
E. Ringe, M. R. Langille, J. Zhang, J. Huang, C. A. Mirkin, R. P. Van Duyne, L. D. Marks, J. Phys. Chem. Lett. (2012) 3, 1479

## Slide 28: Plasmon Length & FWHM
Slope = 3.1(8) meV/nm
Slope = 2.89(10)
Slope = 2.4(3)
Slope = 2.78(11)
Slope = 2.92(8)
Plasmon Length
Side Length
E. Ringe, M. R. Langille, J. Zhang, J. Huang, C. A. Mirkin, R. P. Van Duyne, L. D. Marks, J. Phys. Chem. Lett. (2012) 3, 1479

## Slide 29: Higher Order Modes, Ag
EPL=L/n
1
3
4

## Slide 30: Summary
A lot can be learned from single particle LSPR, particularly when done on many particles and with ~1meV resolution (sorry folks, not just EELS on one or two)
  Trends with size, shape, fine details of structure
Not everything
  We cannot resolve where the hot-spots are

## Slide 31: Grey Haired Comments I

## Slide 32: Surfaces are not trivial
Y. Lin et al, Physical Review letters, 2013. 111, 156101.
1nm
SrO surface
1nm
TiO2 DL (13)
Grown with oleic acid
Grown with acetic acid
Profile imaging, ANL-ACAT

## Slide 33: Grey Hair Comments II
The Howie Challenge
The Marks Challenge
E. Ringe et al., Wulff Construction for Alloy Nanoparticles. Nano Letters 2011, 11, 3399

## Slide 34: Questions ?
Research is to see what everybody else has seen, and to think what nobody else has thought Albert Szent-Györgi