## Slide 1: Tribology in Full View, From Atomic Transfer Layers to Hip Replacements
Laurie Marks
Department of Materials Science and Engineering, Northwestern University, USA

## Slide 2: Energy
“…the greatest source of new energy is the energy we waste today.”
Samuel Bodman, U.S. Secretary of Energy, 2008
Image Source:
John Stringer
Electric Power Research Institute

## Slide 3: Friction
Friction ~5% of GDP
40-50% of power in a new auto engine
http://www.fueleconomy.gov

## Slide 4: Tribology: The study of friction. From Greek “tribein” to rub
Empirically, we do better in reducing friction than the Egyptians, but we certainly do not understand everything.
D. Dowson. History of tribology. Professional Engineering Publishing, London, 2nd edition, 1998

## Slide 5: Friction is from plastic/elastic sliding of asperities
M. Falvo, Physics 267, http://www.physics.unc.edu/~falvo/phys267/index.html

## Slide 6: Experimental Approach

## Slide 7: Simple Examples
Sliding of a W tip on Au: Ploughing
Liquid-like1 deformation of Au (surface diffusion dominated)
1D.W.Pashley, M.H. Jacobs, M.J. Stowell, T.J. Law, Phil Mag 10, 127 (1964); A. Merkle & L.D. Marks, Wear 265, 1864 (2008)
500 nm
50 nm

## Slide 8: Tribological Recrystallization
150nm
Tip
Vacuum
Film
Y. Liao et al, Phil Mag Letts 90 (2010) 219

## Slide 9: Sliding on NFC in wet N2
Localized tribochemical etching by water C+H2O  CO + H2 (water-gas shift)
A. M'ndange-Pfupfu et al, Tribology Letters, 49 (2013) 351.

## Slide 10: Sliding on NFC in H2
Minimal wear, hydrogen passivation
Consistent with “classic” tribochemical opinion
A. M'ndange-Pfupfu et al, Tribology Letters, 49 (2013) 351.

## Slide 11: Arthritis and Hip Replacement
Chart: Cause of Disability (U.S. 2005)
| Arthristis or rheumatism | Back or spine problems | Heart trouble | Lung or respiratory | Mental or emotional problem | Diabetes | Deafness or hearing problem | Stiffness | Blindness or vision problem | Stroke | Cancer | others
 | 19 | 16.8 | 6.6 | 4.9 | 4.9 | 4.5 | 4.2 | 3.6 | 3.2 | 2.4 | 2.2 | 27.7
8.5 M (19%)

## Slide 12: Hip Joint
Rauber/Kopsch: Anatomie des Menschen (1998)
pelvis
femur
cartilage
acetabulum cup
acetabulum
femoral head
femoral stem
www.zimmer.com

## Slide 13: Wear-Mediated Osteolysis
osteoblast
osteoclast/ polymorphonuclear giant cell
http://academic.brooklyn.cuny.edu/biology/bio4fv/page/aviruses/cellular-immune.html
Archibeck, MJ; Jacobs, JJ; Roebuck, KA; Glant, TT. Journal of Bone & Joint Surg, 2000
wear particles
osteolysis
opsonization
phagocytosis
disrupted balance between osteoclasts/PMNs and osteoblasts:
osteoclasts ↑, osteoblasts ↓

## Slide 14: Some Issues
Grain Boundary Corrosion
In-situ Wear
P. Panigrahi et al; Hoffman et al
Liao & Marks, submitted
Liao et al., Science 334, 1687 (2011)
Graphitic Tribolayer
Transfer Layer Castillo et al, submitted

## Slide 15: Tribological Layers on MoM
Carbonaceous layers formed by tribochemical reactions were observed on most of the MoM retrievals (80% of 42 retrievals, Wimmer et al., Wear, 255, 1007, 2003)

## Slide 16: Key Observation
This tribolayer correlates with lower wear, corrosion etc
Implication: this is the triboactive region where sliding takes place
The layer has been assumed to be denatured protein (due to referee) – without proof

## Slide 17: Experimental Method
Follow the Science, not the electron
Biological TEM
  Low-dose (~50 e/Å2 or less) EELS
  Control samples (BCS/Albumin)
  Measure effect of sample preparation & electron dose on controls
Cross-check with Raman
Controls, controls, controls
Not just one measurement

## Slide 18: Tribofilm collection
Tribofilm on #17 retrieval was collected using a nanoprobe in FIB.
Care was taken to minimize the exposure to ion/electron beam.

## Slide 19: Minimize radiation damage
EELS spectrum of the serum dried on copper grid
Dried Bovine Calf Serum

## Slide 20: Graphitic carbon (~82% sp2)
Sample from pole of retrieval, removed due to loosening of the acetabular component (not excessive wear)
58e/Å2

## Slide 21: Graphitization of carbons due to sliding
In-situ
J.C. Sanchez-Lopez et al., Surf. Coat. Tech. 163, 444 (2003)
Merkle, et al. Carbon 48, 587 (2010)
M'Ndange-Pfupfu, et al Diam. Relat. Mat. 20, 1143 (2011)

## Slide 22: HREM: Graphitic carbon
“Classic” basal-plane fringes from graphitic material

## Slide 23: Raman Results
D band (disordered, sp3) at 1388 cm-1
G band (graphitic, sp2) at 1567 cm-1
(Stage 2 graphitic carbon)
Similar results
Different Locations (pole/side of head/cup)
Different Retrievals
Simulator Tests
Blood is different

## Slide 24: Raman Mapping
D
G
Amount of carbon varies in the tribofilm (presumably due to the thickness)
thick region
thin region
substrate

## Slide 25: Raman spectra of carbon
Amorphization trajectory showing variation of the G position and I(D)/I(G) ratio.
Typical Raman spectra of carbon films
Chu and Li, Mater. Chem. Phys, 2006
sp2 carbon > 80%
Nano graphite
Ferrari and Robertson, Phys Rev B, 2000

## Slide 26: Simulator Experiments
Chart: 
Chart: 16N at the edge
Chart: 56N
Chart: 64N
8 N
16 N
56 N
64 N
Raman results show that tribological film is generated when 16N < F < 56N,
consistent with optical/SEM observations.
load
tribofilm

## Slide 27: What it is not
Graphite (short-range ordered sp2/sp3)
It is not temperature (too low)
It is not adventitious carbon (too thin)
It is not beam damage (control experiments)
It is not an artifact of sample preparation (control experiments)
It is not simply mechanical
Athermal effects (x-rays from sellotape), probably not

## Slide 28: What do we know?
It is linked to Mo (not Cr or Co)
Film is yellow/brown, similar to degraded PTFE, hydraulic oil varnish…..
There is an electrochemical link
It requires both sliding and pressure to form
  Not too much, not too little (like vodka)
No evidence of CrOx co-existing with layer (i.e. conditions at metal are reducing)
Albumin is C3076H4833N821O919S42 , and eliminating water, ammonia (and hydrogen sulfide) gives C3076H448 – close to NFC/DLC

## Slide 29: Summary
Much to be done to understand tribology at the nanoscale (fun)
  Long-range elastic/plastic processes can occur
  Local tribochemical processes
  Local wear processes (ultra-low wear) at the monolayer even in hard materials
  Unexpected processes
  Formation of transfer layers which only need to be single layers

## Slide 30: Questions?
Extended Model of Schmaltz, 1936
Input
Basic materials parameters from experiment and/or theory, e.g. sp
Output
Scale independent models without free parameters
Implants