## Slide 1: Dynamical Diffraction
Doing it right
Known, but often ignored
Always used in calculations

## Slide 2: Basics
So far:
  Kinematical (single scattering) model
  Ewald sphere (energy conservation, elastic)
  Simple solutions for diffracted beams, fudge for transmitted
Results:
  Qualitatively correct (thickness fringers, bend contours, strain)
  Quantitatively incorrect
  Incorrect inferences for inelastic

## Slide 3: Notes on History
De Broglie proposed all matter could be written as waves in 1925
Schrödinger expanded to “undulatory mechanics” in 1926
Electron diffraction was demonstrated in 1927-28
Explained (non-relativistically) using dynamical theory by Bethe in 1928.

## Slide 4: Dynamical Diffraction
Fully account for scattering from diffracted beams back to transmitted (and others)
Well understood, but only one useful simplification (two-beam), where result is
Numerical solutions in other cases easy, but it is important to understand why the have their form

## Slide 5
Kinematical
Dynamical

## Slide 6: Math (in notes)

## Slide 17
szeff = (sz2+ 1/eg2)1/2

## Slide 19: 2-Beam solutions
Thickness fringes for zero and larger sz
Bend contours

## Slide 20: Life is eigenvalues/vectors
Walk to Car
Drive Down LSD
Watch the Game
Going from Evanston to watch a Bears game (we can always hope)
Individuals or collective – different eigenvectors of the trip
Walk to Seats

## Slide 21: An aside
Everything is an “***on”
  Phonons, electrons, magnons…
They are called “quasiparticles”, effectively independent solutions (eigenfunctions) in quantum mechanics.
The plane waves in kinematical are not “**ons”, as they are changing.

## Slide 23
Key point: look at the +/- cases:
b(k+,r) = 2Co exp(2pig+z)exp(pi[2k++g] .r)cos(pg.r)
|b(k+,r)|2  cos(pg.r)2 |b(k-,r)|2  sin(pg.r)2
Damped Strongly Damped Weakly

## Slide 24: Top-Bottom Effect
+/-
+  ++/-+
-  --/+-
-+/--
-
+-/--
-
+-/--
--
Type of Bloch Wave
Type before defect
+ Strongly Adsorbed
Defect scatters Bloch waves (inclined)
+ Damped
e-
Image

## Slide 26
ALCHEMI
Atom Location by Channeling Enhanced Microanalysis
Cherns, Howie and Jacobs, 28a, Naturforschung, 1973

## Slide 28
Au [110] – Vacuum wave
Courtesy C. Kisielowski, J.R. Jinschek (NCEM, Berkeley)

## Slide 29: But…column approximation?
t, 20nm
w
w = 2tq. Take q=10 mRad, t=20nm, w=4 Angstroms

## Slide 30: Basis Sets
Plane waves
  Solutions in vacuum
  Used in kinematical theory
Bloch waves
  Used in 2-beam theory (and beyond)
  Combinations of plane waves
Tight-binding model
  Uses atom-like orbitals (similar to chemistry, MO)

## Slide 31: Basis Sets Continued
What to use?
No simple answer
The one which gives the simplest explanation with the least complications (KISS = Occam’s Razor) is normally best
Often this changes depending upon the type of problem/property of interest…

## Slide 32: Channeling: Real-Space model
* Fujimoto, phys. stat. sol. (1978) + many others
Van Dyck and Op de Beeck, Ultramicroscopy (1996)
Electron channeling approximation*:
  1) Ignore all but ZOLZ interactions (high energy)
  2) Assume sample orientation so that one has well separated atomic columns along z (in initial expansion only)
  3) Use atomic-column based tight-binding model

## Slide 33: Channeling Concept
For many zone axes, in projection atoms are well separated
Potential large near columns
Small between columns
Chart: 
| -1 | -0.9 | -0.8 | -0.70000000000000007 | -0.60000000000000009 | -0.50000000000000011 | -0.40000000000000013 | -0.30000000000000016 | -0.20000000000000015 | -0.10000000000000014 | -1.3877787807814457E-16 | 9.9999999999999867E-2 | 0.19999999999999987 | 0.29999999999999988 | 0.39999999999999991 | 0.49999999999999989 | 0.59999999999999987 | 0.69999999999999984 | 0.79999999999999982 | 0.8999999999999998 | 0.99999999999999978 | 1.0999999999999999 | 1.2 | 1.3 | 1.4000000000000001 | 1.5000000000000002 | 1.6000000000000003 | 1.7000000000000004
 | -4.1292e-07 | -2.04e-05 | -0.00055308 | -0.0082297 | -0.067206 | -0.30119 | -0.74082 | -1 | -0.74082 | -0.30119 | -0.067206 | -0.0082297 | -0.00055309 | -2.0812e-05 | -2.0812e-05 | -0.00055309 | -0.0082297 | -0.067206 | -0.30119 | -0.74082 | -1 | -0.74082 | -0.30119 | -0.067206 | -0.0082297 | -0.00055308 | -2.04e-05 | -4.1292e-07
V(r) Atoms
~0
r

## Slide 34: Consider an isolated column: I
e-
d
Average potential

## Slide 36: Final form, almost
Spreading of information
Diffraction

## Slide 37
Look for a solution of form
This leads to

## Slide 38: Consider an isolated column: II
Problem reduces to 2-D Schrödinger's Eqn
Solutions have form:
2D orbitals
“Transverse Energy”

## Slide 39: Character of States
2D analogues of 3D atomic orbitals
1s 2p 3d

## Slide 40: Dynamical Solutions: many columns
General solution
On a zone (symmetry), s-type orbitals dominate
Not so simple if the zone axis is complicated – not a solved problem

## Slide 41
light atoms
heavy atoms
light atoms
heavy atoms
Curtesy D. Van Dyck

## Slide 42: Probe Channeling
z=0 nm
z=10 nm
z=33.0 nm
z=23.5 nm

## Slide 43: Heavy atoms first, then light

## Slide 44: Depth dependence by atom type
0
200
400
600
800
1000
Thickness [Å]
O
Al
Ga
|1-y(r)| at atom

## Slide 45: OPW
Suppose we have some atomic-like state,
and also add a plane-wave like term
The two must be orthogonal – a plane wave is not
Instead use
This is small when is large, misses the core

## Slide 46: So what does this gain us?
First core state (1s) cancels most of potential (OPW)
Only need to consider a few states, unlike classic Bloch-wave methods
N.B. Tight-binding
Chart: 
| -1 | -0.9 | -0.8 | -0.70000000000000007 | -0.60000000000000009 | -0.50000000000000011 | -0.40000000000000013 | -0.30000000000000016 | -0.20000000000000015 | -0.10000000000000014 | -1.3877787807814457E-16 | 9.9999999999999867E-2 | 0.19999999999999987 | 0.29999999999999988 | 0.39999999999999991 | 0.49999999999999989 | 0.59999999999999987 | 0.69999999999999984 | 0.79999999999999982 | 0.8999999999999998 | 0.99999999999999978 | 1.0999999999999999 | 1.2 | 1.3 | 1.4000000000000001 | 1.5000000000000002 | 1.6000000000000003 | 1.7000000000000004
 | -4.1292e-07 | -2.04e-05 | -0.00055308 | -0.0082297 | -0.067206 | -0.30119 | -0.74082 | -1 | -0.74082 | -0.30119 | -0.067206 | -0.0082297 | -0.00055309 | -2.0812e-05 | -2.0812e-05 | -0.00055309 | -0.0082297 | -0.067206 | -0.30119 | -0.74082 | -1 | -0.74082 | -0.30119 | -0.067206 | -0.0082297 | -0.00055308 | -2.04e-05 | -4.1292e-07
 | -1 | -1 | -1 | -0.99994 | -0.99616 | -0.92289 | -0.53351 | -0.15 | -0.53351 | -0.92289 | -0.99616 | -0.99994 | -1 | -1 | -1 | -1 | -0.99994 | -0.99616 | -0.92289 | -0.53351 | -0.15 | -0.53351 | -0.92289 | -0.99616 | -0.99994 | -1 | -1 | -1
 | -4.1292e-07 | -2.0399e-05 | -0.00055282 | -0.0081722 | -0.063366 | -0.22408 | -0.27433 | -0.15 | -0.27433 | -0.22408 | -0.063366 | -0.0081722 | -0.00055283 | -2.0812e-05 | -2.0812e-05 | -0.00055283 | -0.0081722 | -0.063366 | -0.22408 | -0.27433 | -0.15 | -0.27433 | -0.22408 | -0.063366 | -0.0081722 | -0.00055282 | -2.0399e-05 | -4.1292e-07
1s state
Potential
Effective (pseudo) potential

## Slide 47: A Quick Comparison
Bloch Wave
  Different States
  Oscillate with Depth
Interference
  Thickness Fringes,etc
Tight Binding
  Atomic States
  Oscillate with Depth
Interference
  Atomic contrast
Note: ignore overlap of states

## Slide 48: Channeling Concept
Lowest Transverse Energy states (1s) dominate
Can ignore (to 2nd order) delocalized states
Chart: 
| -1 | -0.9 | -0.8 | -0.70000000000000007 | -0.60000000000000009 | -0.50000000000000011 | -0.40000000000000013 | -0.30000000000000016 | -0.20000000000000015 | -0.10000000000000014 | -1.3877787807814457E-16 | 9.9999999999999867E-2 | 0.19999999999999987 | 0.29999999999999988 | 0.39999999999999991 | 0.49999999999999989 | 0.59999999999999987 | 0.69999999999999984 | 0.79999999999999982 | 0.8999999999999998 | 0.99999999999999978 | 1.0999999999999999 | 1.2 | 1.3 | 1.4000000000000001 | 1.5000000000000002 | 1.6000000000000003 | 1.7000000000000004
 | -4.1292e-07 | -2.04e-05 | -0.00055308 | -0.0082297 | -0.067206 | -0.30119 | -0.74082 | -1 | -0.74082 | -0.30119 | -0.067206 | -0.0082297 | -0.00055309 | -2.0812e-05 | -2.0812e-05 | -0.00055309 | -0.0082297 | -0.067206 | -0.30119 | -0.74082 | -1 | -0.74082 | -0.30119 | -0.067206 | -0.0082297 | -0.00055308 | -2.04e-05 | -4.1292e-07
V(r) En
2s
1s

## Slide 49: Full wave
Br
4nm
19nm
11nm
26nm
Br
Real Imaginary
Cu

## Slide 50: Full wave
4nm
19nm
Br
Real Imaginary
4nm
Cu

## Slide 51: |1-y(r)|
4nm
.4nm
11nm
19nm
26nm
34nm
Br
Carbon is more important than Bromine for ~ 10nm

## Slide 52
Sinkler Plots: Quasi-Kinematical
(r)-1 has atom-like peaks with species-dependent oscillation
r)-1, 25 Å
Real
Imaginary
r)-1, 125 Å
Note: if the points lay on a straight line the result is pseudo-kinematical, i.e. it walks and talks like kinematical even though it is not

## Slide 53: Thickness Movie
Oxygen 1s States
Metal 1s States

## Slide 54
Bloch-wave formulation (dynamical theory)
Wave function of the incident electron:
Ψ(r) = Σj ε(j) b(j)(r)
Bloch state (eigen state):
b(j)(r) = ΣgCg (j)exp[2πi(k(j)+g)·r]
Schroedinger equation
Electron density distribution of the Bloch state: |b(j)(r)|2
Excitation of the Bloch states: ε(j)

## Slide 55
Dispersion surface and Excitations of Bloch states
SrTiO3 [001]
Dispersion surface
Excitations of the branches
(Energy conservation)
100kV
Branches with lower potential energy
Higher kinetic energy (k)
kz
|ε(j)|2
Curtesy of K. Tsuda

## Slide 56
PbZrO3 [001]
Bloch-state
simulations
⇒
⇒ : well-excited
at ZA
⇒
⇒
100kV

## Slide 57: Caveats
In a thick crystal, must include all states
Higher En states not so “atomic”
Overlap of states on different columns can be important
Tilt off zone axis  excites more p, d states
Strain=tilt, hence may destroy simple picture

## Slide 58: Relevance 1: HREM
For a thin sample the 1s states dominate – simple
The scattering is pseudo-kinematical, easy to interpret
In thicker samples (> 20nm) not quite so simple

## Slide 59: Examples
MTP (1983)
SrTiO3 (001) (2015)
1nm
TiO2 DL

## Slide 60
Au [110] – Vacuum wave
Courtesy C. Kisielowski, J.R. Jinschek (NCEM, Berkeley)

## Slide 61: Relevance 2: ADF
The closer the electron comes to the nucleus, the higher the probability of high-angle scattering (elastic or inelastic)
1s states dominate the high-angle scattering

## Slide 62: Probe Channeling
z=0 nm
z=10 nm
z=33.0 nm
z=23.5 nm

## Slide 63
Strain Contrast at Si/SiO2 Interfaces
David Muller 2001
50 mrad
25 mrad
c-Si
SiO2
a-Si
(JEOL 2010F, 200 kV, Cs=1mm)
Strain Fields cause dechanneling (and scattering to small angles)
ADF Inner angle:
Z. Yu, D. A. Muller, and J. Silcox, J. Appl. Phys. 95, 3362 (2004).

## Slide 64: When Does the Simple Picture Work?
Simple incoherent, Z1.7 theory works well:
  for an amorphous specimen
  for randomly-oriented polycrystalline specimens
  (mostly) for single crystals tilted between major zone axes
It doesn’t work for single crystals oriented on a zone axes – i.e. when you get atomic-place resolution.