## Slide 1: Precession Diffraction: The Philospher’s Stone of Electron Crystallography?

## Slide 2: Focus
Many methods exist for obtaining diffraction information
  Selected Area
  Nanodiffraction and variants
  CBED
All are complicated to interpret
Reciprocal space is right, but intensities depend upon thickness, tilt etc

## Slide 3: What PED can do
We would like a method where not just the positions of the spots, but also the intensities could be used.
Not rigorously equivalent to simple kinematical diffraction, but has many similarities
  If the structure factor is large  Intensity is large
  Useful for fingerprinting structures
  Often does not need calculations to interpret

## Slide 4
History – Electron Precession (1993)
e-
e-


Advantages:

## Slide 5
Scan
De-scan
Specimen
Conventional Diffraction Pattern
Precession…
Precession Diffraction Pattern
(Ga,In)2SnO5 Intensities
412Å crystal thickness
Non-precessed
Precessed
(Diffracted amplitudes)

## Slide 6: Precession System
US patent application:
“A hollow-cone electron diffraction system”.
Application serial number 60/531,641, Dec 2004.

## Slide 7
Can be easily retrofitable to any TEM 100- 300 KV
precession is possible for any beam size 300 - 50 nm
Precession is possible for a parallel or convergent beam
precession eliminates false spots to ED pattern that belong to dynamical contributions
precession angle can vary continuously (0°-3°) to observe true crystallographic symmetry variation
Software ELD for easy quantification of ED intensities and automatic symmetry ( point, space group ) research
SPINNING STAR : UNIVERSAL INTERFASE FOR PRECESSION ELECTRON DIFFRACTION FOR ANY TEM ( 120 -200 -300 KV )
Easily interfaced to electron diffractometer for automatic 3D structure determination

## Slide 8: Examples:
Complicated Structures
  Hard to interpret SAED
  Simple to interpret PED
EDS
  Elemental ratio’s depend upon orientation in standard mode
  Weak to no dependence with PED

## Slide 9
APPLICATION : FIND TRUE CRYSTAL SYMMETRY
PRECESSION OFF
IDEAL KINEMATICAL (111)
UVAROVITE (111)
PRECESSION ON
Courtesy M.Gemmi
Univ of Milano

## Slide 10
APPLICATION : PERFECT CRYSTAL ORIENTATION
PRECESSION OFF
PRECESSION ON
Crystals –specially minerals -usually grow in platelet
or fiber shape and results dificult to orient perfectly in a particular zone axis; in this example olivine crystals are perfectly oriented after precession is on.
OLIVINE
Courtesy X.Zou, S.Hovmoller Univ Stockholm

## Slide 11: Carbide

## Slide 12: Crystal Structures of STO and Fe2MnAl
STO (Perovskite)
Fe2MnAl (L21-ordered)
Fe
Mn
Al
Ti
O
Sr
Notes: Ordered oxide and intermetallics.

## Slide 13: PED-EDS in ALCHEMI Type Measurements
Reduced electron channeling effects (g=200 for both cases)
Orientation-insensitive chemistry measurement
SrTiO3
Fe2MnAl
Liao and Marks, Ultramicroscopy, 126, 2013
Notes: Channeling obtained by setting a standing electron wave across the structure. Alchemi is first proposal by Tafto and Spence, 218, Science, 1982; Tafto and Spence, 9, Ultramicroscopy, 1982.

## Slide 14: Effects of Precession Angle
Sr/Ti increases with increasing precession angle when θ <23 mrad.
Sr/Ti is ~1 when θ > 23 mrad.
Liao and Marks, Ultramicroscopy, 126, 2013
Notes: higher angle results in less dynamical effects. It depends on material species, orientation and presumably thickness.

## Slide 15: PED-EELS ?
Signal is enhanced for zone-axis PED-EELS
Signal is reduced for two-beam PED-EELS
In both cases, Ti/O ratio is unchanged
Two-beam
Zone-axis
Estrade et al., Ultramicroscopy, 2012

## Slide 16: Practical Use
Two commercial systems (one hardware, another software) are available
Not complicated, and could probably be written in scripting language
Alignment can be tricky – it always is
Not rocket science, to use

## Slide 17: Some Practical Issues
Bi-polar push-pull circuit (H9000)
Projector Spiral Distortions (60 mRad tilt)

## Slide 18
Block Diagram
‘Aberrations’
e-
e-



## Slide 19: Remember the optics
Sample
Objective Postfield
Objective Prefield
Better Diagram
Postfield Misaligned
Idealized Diagram
Descan
Scan

## Slide 20
Sample
Objective Postfield
Objective Prefield
Descan
Scan
Correct Diagram
Both Misaligned
Idealized Diagram
Remember the optics

## Slide 21: Alignment can be tricky

## Slide 22: Why?
Although PED has been around since 1992, and very actively used for ~10 years (mainly in Europe), there is no simple explanation (many have tried and failed)
Explanation is a bit rocket science

## Slide 23: Why?
What, if any generalizations can be made?
Role of Precession Angle
  Systematic Row Limit
Importance of integration
  Phase insensitivity
  Important for which reflections are used
  Fast Integration Options

## Slide 24: Ewald Sphere Construction
z
0
g
k
s
k+s
sz
Scan
De-scan
Specimen
(Diffracted amplitudes)

## Slide 25: Levels of theory
Precession integrates each beam over sz
Full dynamical theory
  All reciprocal lattice vectors are coupled and not seperable
Partial dynamical theory (2-beam)
  Consider each reciprocal lattice vector dynamically coupled to transmitted beam only
Kinematical theory
  Consider only role of sz assuming weak scattering
Bragg’s Law
  I = |F(g)|2

## Slide 26: Early Models
Iobs depends upon |F(g)|, g, f (precession angle) which we “correct” to the true result
Options:
0) No correction at all, I=|F(g)|2
1) Geometry only (Lorentz, by analogy to x-ray diffraction) corresponds to angular integration
2) Geometry plus multiplicative term for |F(g)|

## Slide 27: Bragg’s Law fails badly (Ga,In)2SnO5
3.2 Å; R=0.02
50 Å; R=0.19
100 Å; R=0.25
200 Å; R=0.49
400 Å*; R=0.78
800 Å; R=0.88

## Slide 28: Kinematical Lorentz Correction
I(g) =ò |F(g) sin(ptsz)/(psz) |2 dsz
sz taken appropriately over the Precession Circuit
t is crystal thickness (column approximation)
f is total precession angle
I(g) = |F(g)|2L(g,t,f)
K. Gjønnes, Ultramicroscopy, 1997.

## Slide 29: Kinematical Lorentz correction: Geometry information is insufficient
Need structure factors to apply the correction!
Fkin
Fcorr

## Slide 30: 2-Beam (Blackman) form
Limits:
  Ag small; Idyn(k) µ Ikin(k)
  Ag large; Idyn(k) µ ÖIkin(k) = |Fkin(k)|
But…
This assumes integration over all angles, which is not correct for precession (correct for powder diffraction)

## Slide 31: Blackman Form

## Slide 32: Blackman+Lorentz
Alas, little better than kinematical
Comparison with full calculation, 24 mRad
Angstroms

## Slide 33: Two-Beam Form
I(g) = ò | F(g) sin(ptseffz)/(pseffz) |2 dsz
sz taken appropriately over the Precession Circuit
szeff = (sz2 + 1/xg2)1/2
Do the proper integration over sz (not rocket science)

## Slide 34: Two-Beam Integration: Ewald Sphere
Small (hkl)
Large (hkl)
Medium (hkl)

## Slide 35: 2-Beam Integration better
3.2 Å; R=0.02
50 Å; R=0.19
100 Å;R=0.24
200 Å; R=0.44
400 Å*; R=0.62
800 Å; R=0.67

## Slide 36: Some numbers
R-factors for 2-beam model
R-factors for kinematical model
See Sinkler, Own and Marks, Ultramic. 107 (2007)

## Slide 37: Fully Dynamical: Multislice
“Conventional” multislice (NUMIS code, on cvs)
Integrate over different incident directions 100-1000 tilts
f = cone semi-angle
  0 – 50 mrad typical
t = thickness
  ~20 – 50 nm typical
  Explore: 4 – 150 nm
g = reflection vector
  |g| = 0.25 – 1 Å-1 are structure-defining
2f
t

## Slide 38: Multislice Simulation
Multislice simulations carried out using 1000 discrete tilts (8 shown) incoherently summed to produce the precession pattern1
How to treat scattering?
Doyle-Turner (atomistic)
Full charge density string potential -- later
1 C.S. Own, W. Sinkler, L.D. Marks Acta Cryst A62 434 (2006)

## Slide 39: Multislice Simulation: works (of course)
R1 ~10% without refinement of anything

## Slide 40: Global error metric: R1
Broad clear global minimum – atom positions fixed
R-factor = 11.8% (experiment matches simulated known structure)
  Compared to >30% from previous precession studies
Accurate thickness determination:
  Average t ~ 41nm (very thick crystal for studying this material)
(Own, Sinkler, & Marks, in preparation.)

## Slide 41: Quantitative Benchmark: Multislice Simulation
0mrad
10mrad
24mrad
75mrad
Experimental dataset
Error
g
thickness
(Own, Sinkler, & Marks, in preparation.)
Absolute Error = simulation(t) - kinematical
50mrad
Bragg’s Law

## Slide 42: Partial Conclusions
Separable corrections fail; doing nothing is normally better
Two-beam correction is not bad (not wonderful)
Only correct model is full dynamical one (alas)
N.B., Other models, e.g. channelling, so far fail badly – the “right” approximation has not been found

## Slide 43: Overview
What, if any generalizations can be made?
Role of Precession Angle
  Systematic Row Limit
Importance of integration
  Phase insensitivity
  Important for which reflections are used

## Slide 44: Role of Angle: Andalusite
Natural Mineral
  Al2SiO5
  Orthorhombic (Pnnm)
    a=7.7942
    b=7.8985
    c=5.559
  32 atoms/unit cell
Sample Prep
  Crushm Disperse on holey carbon film
  Random Orientation
2 C.W.Burnham, Z. Krystall. 115, 269-290, 1961

## Slide 45: Measured and Simulated Precession patterns
Bragg’s Law Simulation
Precession Off
6.5 mrad
13 mrad
18 mrad
24 mrad
32 mrad
Experimental
Multislice

## Slide 46: Decay of Forbidden Reflections
Decay with increasing precession angle is exponential
  The non-forbidden (002) reflections decays linearly
 | D(001) | D(003)
Experimental | 0.109 R2=0.991 | 0.145 R2=0.999
Simulated (102nm) | 0.112 R2=0.986 | 0.139 R2=0.963
Simulated 28-126 nm | 0.112±0.012 | 0.164±0.015
Rate of decay is relatively invariant of the crystal thickness
Slightly different from Jean-Paul’s & Paul’s – different case

## Slide 47: Quasi-systematic row
Projection of
Incident beam
Precession
Systematic Row
Forbidden, Allowed by Double Diffraction
On-Zone
Precessed

## Slide 48: Evidence: 2g allowed
Rows of reflections arrowed should be absent (Fhkl = 0)
Reflections still present along strong systematic rows
Known breakdown of Blackman model
Si [110]
Si [112]
e-
e-



## Slide 49: Phase and Averaging
For each of the incident condition generate 50 random phase sets {f} and calculate patterns:
Single settings at 0, 12, 24 and 36 mrad (along arbitrary tilt direction).
At fixed semi-angle (36 mrad) average over range of a as follows:
3 settings at intervals of 0.35º
5 settings at intervals of 0.35º
21 settings at intervals of 1º
For each g and thickness compute avg., stdev:
+
+
+
+
0 mrad
12
24
36
+
+
+
+

## Slide 50: Phase independence when averaged
single setting
3 settings, 0.35º interval
5 settings, 0.35º interval
21 settings, 1º interval (approaching precession)
Sinkler & Marks, 2009

## Slide 51: Why does it work?
If the experimental Patterson Map is similar to the Bragg’s Law Patterson Map, the structure is solvable – Doug Dorset
If the deviations from Bragg’s Law are statistical and “small enough” the structure is solvable – LDM

## Slide 52: Why is works - Intensity mapping
Iff Iobs(k1)>Iobs(k2) when Fkin(k1) > Fkin(k2)
  Structure should be invertible (symbolic logic, triplets, flipping…)

## Slide 53: Suggested PED flowchart

## Slide 54: Preprocess?
Kinematical (reference)
“Good” Region
Precession pattern (experiment)
f = 24mrad

## Slide 55: Speculation…
Generate initial structure estimate
  Use 2-beam approximation to invert/correct
  Partial refinement, using 1/2 kpoint Bloch-Wave method (preprint will be on Los Alamos server soon); large residue least-squares code (e.g. dmnf from Port library)
  Final full refinement using 25-100 beam BW (+Bethe terms, e.g. Stadleman + dmnf)

## Slide 56: Hypothesis: Thickness ranges
(not so easy)

## Slide 57: Summary
PED is
  Approximately Invertable
  Pseudo Bragg’s Law
  Approximately 2-beam, but not great
  Properly Explained by Dynamical Theory
PED is not
  Pseudo-Kinematical (this is different!)
  Fully Understood by Dummies, yet

## Slide 58: Questions ?