## Slide 1: The Phase Problem for Electrons
L. D. Marks
Northwestern University
Electron Crystallography is the branch of science that uses electron scattering and imaging to study the structure of matter

## Slide 2: What is the science?

## Slide 3: Why determine the structure?
To finish my PhD
To get/keep my job
Because structure coupled with other science really matters – but only when coupled
Follow the science, not the electron

## Slide 4: Metal-on-Metal Hip Replacements
4
Alloys show differential corrossion in Bovine Calf Serum, attack at some grain boundaries and matrix carbides
SEM Image
Pooja Panigrahi, undergraduate thesis, 2011

## Slide 5: Carbides
54.7
-1-11
333
-200
-600
ZA [011]
What are the carbides (currently unclear)? Do different carbides corrode differently in humans?
Yifeng Liao et al, submitted

## Slide 6: Solid Oxide Fuel Cells
La0.84Sr0.16Cr0.45Pd3.61Ox
Pd ~ 71%
Pd nanoparticles formed in-situ have much better performance
Yougui Liao et al, submitted

## Slide 7: Thermodynamic Shape Control
7
Enterkin, J. A et al, Nano Lett. 11, 993 (2011); ACS Catalysis, 1 (6), 629, 2011
Substrate
Chart: Temperature (°C)
| 25 | 50 | 75 | 100 | 125 | 150 | 175 | 200 | 225 | 250 | 275 | 300 | 325 | 350 | 375 | 400 | 425 | 450 | 475 | 500 | 525 | 550
Nanocubes Cycle 1 | 0 | 0 | 0 | 0 | 0 | 0.59132 | 1.9706 | 6.2393 | 21.3693 | 58.6607 | 75.2656 | 85.3478 | 91.2173 | 95.6237 | 97.8908 | 99.2388 | 100.0211 | 100.1789 | 99.9559 | 99.9618 | 100.5067 | 100.2013
Nanocubes Cycle 2 | 0 | 0 | 0 | 0 | 0.12506 | 0.66742 | 2.5068 | 7.8454 | 37.0971 | 62.0384 | 75.394 | 84.5059 | 90.0892 | 93.6365 | 96.5822 | 98.4803 | 99.5066 | 100.0231 | 100.2119 | 100.4662 | 100.1684 | 100.5609
Nanocubes Cycle 3 | 0 | 0 | 0 | 0 | 0.23957 | 0.64074 | 2.2422 | 7.3214 | 28.1959 | 56.2254 | 69.1507 | 78.9498 | 85.1363 | 89.8721 | 93.2419 | 95.6559 | 97.3368 | 98.6955 | 99.6002 | 99.7891 | 100.4768 | 100.6423
Nanocubes Cycle 4 | 0 | 0 | 0 | 0 | 0 | 0.56038 | 2.0502 | 7.2643 | 29.3597 | 55.4226 | 69.1758 | 77.9196 | 84.306 | 88.4441 | 91.7451 | 94.3038 | 96.3328 | 97.7205 | 99.0418 | 98.808 | 99.2207 | 99.7945
Powder Cycle 1 | 0 | 0 | 0 | 0 | 0 | 0.31169 | 0.36732 | 0.94058 | 1.8945 | 4.2965 | 8.5154 | 15.3258 | 25.3904 | 36.5296 | 47.3075 | 56.1887
Powder Cycle 2 | 0 | 0 | 0 | 0 | 0 | 0 | 0.53751 | 0.9932 | 2.4026 | 5.0151 | 9.4394 | 16.3008 | 25.3412 | 35.5785 | 45.2132 | 54.9185
Powder Cycle 3 | 0 | 0 | 0 | 0 | 0 | 0.14959 | 0.45555 | 1.1941 | 2.361 | 5.0269 | 9.369 | 16.4134 | 25.8246 | 36.1987 | 46.3036 | 55.8707 | 64.0287 | 70.4759 | 75.8885 | 79.6901 | 82.853 | 85.2465
Powder Cycle 4 | 0 | 0 | 0 | 0 | 0 | 0 | 0.60244 | 1.0792 | 2.3401 | 4.4779 | 8.2964 | 13.4538 | 20.0931 | 27.293 | 34.2376 | 41.3249 | 47.3833 | 53.0104 | 58.7655 | 64.6375 | 70.6224 | 77.0633
Cycle 1 | 1
Cycle 2 | 1
Cycle 3 | 1
Cycle 4 | 1
More reactive (propane oxidation)
SrTiO3 (001) surface dictates epitaxy nanoparticles  catalysis
Pt
SrTiO3

## Slide 8: How to solve a structure?
Guess, then refine
  Will always give something, but if the guess is wrong GIGO
Use Patterson function
  Difficult for complicated structures (more to come)
Use DFT1
  If the original guess is wrong, GIGO
  Functionals are inaccurate for most oxides (energies wrong)
Get an image
  STM is hard to interpret
  HREM, can be ambiguous (more to come)
Get a Diffraction Pattern
  Incomplete information (more to come)
1For later today

## Slide 9: Four basic elements are required to solve a recovery problem
1. A data formation model
  Imaging/Diffraction/Measurement
2. A priori information
The presence of atoms or similar
3. A recovery criterion:
  A numerical test of Goodness-of-Fit
4. A solution method.
  Mathematical details
Patrick Combettes, (1996). Adv. Imag. Elec. Phys. 95, 155

## Slide 10: Four basic elements are required to solve a recovery problem
1. A data formation model
  Imaging/Diffraction/Measurement
  Kinematical Theory/Linear Imaging
  Single Weak Scattering + Ewald Sphere
  Qualitatively correct; Quantitatively inaccurate
  Bragg’s Law
  Single Scattering + Zero Excitation Error
  Worse than Kinematical Theory (it is different)
  Dynamical Theory/Non-Linear Imaging
  Quantitatively correct, to the accuracy of the electrostatic potential (exact in principle)
Warning: Errors in the model introduce systematic errors in the recovery which of course can lead to GIGO

## Slide 11
(x, y, z)
x
y
(u v w)
u
v
(u v w)
Patterson Function I (FT of Diffraction Pattern)

## Slide 12: Patterson Function II
x
y
u
v
Patterson map will contain points corresponding to vectors between atoms in the real cell
Real Cell
Patterson Cell
Solids normally contain well-separated atoms, and majority of scattering is near the core -- peaked

## Slide 13
Real Cell
Patterson Cell
1) Patterson is symmetric about origin (centrosymmetry)
3) Contains N(N-1) peaks (not counting origin)  gets complicated!
2) Can see pattern of real cell in Patterson cell repeated N times
Patterson Function

## Slide 14: Patterson Function
J Vac Sci Technol A3, 1502 (1986) > 1800 Citations

## Slide 15: Diffraction Phase Problem
F(h) = |F(h)|exp[2i(h)]
FFT
Surface r(r)
Unmeasured
Measured diffraction intensities
|F(h)| = [I(h)]1/2
An equal opportunity problem – true for x-ray and electron diffraction

## Slide 16: Basics
We know the amplitudes
We want to find the phases
Problem is insolvable without additional information – constraints
Use an iterative approach

## Slide 17: The Phase Problem
We have an exit wave from the sample
  y(r) wave in real space = a(r)exp(-if(r))
  Y(u) = òexp(-2piu.r)y(r)dr = A(u)exp(-if(u))
Observables
  I(r) = <|y(r)|2> = <a(r)2> Real Space Image
  I(u) = <|Y(u)|2> = <A(u)2> Diffraction Pattern
Note: “<>” is average over incoherent aberrations and other statistical terms

## Slide 18: Phase: Apples & Oranges
FT Aa exp(-i a)
Ao exp(-i a) IFT
FT Ao exp(-i o)
+
{
Oranle ?
Appge ?
Phase of Apple + Amplitude of Orange = ?

## Slide 19: Phase of Apple = Apple
FT-1 {Ao exp(-i a) }
Apple
Phase is more important than amplitude

## Slide 20: The importance of phase information
Correct Modulus Random Phases
Correct Phase Random Modulus
Suzy

## Slide 21: Role of error in phases (degrees)
0 10 20
30 40 50
We would like to find the phases exactly, but we don’t have to

## Slide 22: Phase and Modulus Errors
0 10° 20° 30° 40°
R 0 26% 52% 78% 104%
Phase Error
Modulus Error
We only need approximately correct phases We can tolerate modulus errors
Modulus Correct
Phase Correct

## Slide 23: How do we overcome this
Recover phase information from a series of images at different defocus.
  Classic inversion problem which can be ill-conditioned
Recover phase information for special cases where solution is exact (in principle)
Recover approximate phase information using constraints (direct methods)

## Slide 24: Inversion
I(r) ~ òY(u)T(u)exp(2piu.r)du + noise
write A(u)=Y(u)T(u)
The optimal filter (L2) F(u) to apply is given by (Wiener, 1940)
F(u) = T*(u)/{|T(u)|2+n(u)2/S(u)2}
n(u) = spectral distribution of noise
S(u) = estimate of signal

## Slide 25: Wiener Filtering
Original Test Object
Linear CTF (close to correct)
Aberrated Image
Wiener Filtered
Simple Example

## Slide 26
Aberration control & reconstruction of electron wave function
illumination tilt series
hardware
feedback
ATLAS
through-focus series
TrueImage
software correction of residual aberrations
Aberration Function χ(g)
Wave Function Ψ(r)
FZ Jülich
Curtesy Rafal Dunin-Borkowski
Notes: 26

## Slide 27
ATLAS & TrueImage:: Stacking Faults in SrTiO3 (110)
Zopt micrograph
Titan 80-300
deficiencies:
shaded columns
inf. signal-to-noise ratio
spurious contrast peaks
[001]
[110]
-
1.38 Å
Ti
O
J. Barthel, PhD Thesis (2007)
Curtesy Rafal Dunin-Borkowski
Notes: 27

## Slide 28
uncorrected phase image
Titan 80-300
deficiencies:
shaded columns
ATLAS & TrueImage:: Stacking Faults in SrTiO3 (110)
1.38 Å
Ti
O
[001]
[110]
-
J. Barthel, PhD Thesis (2007)
Curtesy Rafal Dunin-Borkowski
Notes: 28

## Slide 29
corrected phase image
Titan 80-300
deficiencies:
none
ATLAS & TrueImage:: Stacking Faults in SrTiO3 (110)
1.38 Å
Ti
O
[001]
[110]
-
J. Barthel, PhD Thesis (2007)
Curtesy Rafal Dunin-Borkowski
Notes: 29

## Slide 30: Exact Cases
Suppose we have N pixels, and N/2 are known to be zero (compact support)
Wave is described by N/2 moduli, N/2 phases (for a real wave) in reciprocal space
Unkowns – N ; measurements N/2 ; contraints N/2
Problem is in principle fully solveable
(It can be shown to be unique in 2 or more dimensions, based upon the fundamental theorem of algebra)

## Slide 31: Example: Diffractive Imaging
True diffraction pattern for small particle model
(Non-Convex Constraint)
+
= ?
Convex Support
Constraint
|(x,y)|=1
|(x,y)|=?

## Slide 32: Example: Diffractive imaging
Constraint: part of real-space x is zero
(Convex constraint)
Iteration
  x = 0, part of map
  |X| = |Xobserved|
Iterate

## Slide 33: Phase Recovery
Reconstructed exit wave after 3000 iterations
True real space exit wave for small particle model

## Slide 34: Electron Nanoprobe formation
Lower Objective
Specimen
Condenser Lens III
Back Focal Plane
10 mm aperture -> 50 nm beam
M = 1/200
JM Zuo et al, Science 300, 1419 (2003)

## Slide 35
Coherence length > 15 nm
Convergence angle <0.2 mrad

## Slide 36: Direct Methods vs. Indirect Methods
Indirect Methods:
“Trial and Error”
Direct Methods:
Using available information
to find solutions

## Slide 37: Implementation
Infinite Number of Possible
Arrangements of
Atoms
Finite
R, 2, structure, DFT and chemistry
Direct Methods

## Slide 38: Caveat: Not Physics
This is probability, not an exact “answer”
All one can say is that the “correct” answer will be among those that are found

## Slide 39: What do D.M. give us
With the moon in the right quarter -- real space potential/charge density
In other cases:
  Atom positions may be wrong (0.1-0.2 Å)
  Peak Heights may be wrong
  Too many (or too few) atoms visible
But... this is often (not always) enough to complete the structure
Chris Gimore

## Slide 40: Additional Information Available
Physical nature of experiment
  Limited beam or object size
Physical nature of scattering
  Atomic scattering
Symmetry (sometimes) + unit cell
Statistics & Probability
  Minimum Information/Bias = Maximum Entropy

## Slide 41: Basic Ideas
There are certain relationships which range from exact to probably correct.
Simple case, Unitary Sayre Equation, 1 type
Divide by N, #atoms & f(k), atomic scattering factors
Constraint
Sayre, D. Acta Cryst. 5, 60, 1952

## Slide 42: Real/Reciprocal Space
-2
1
U(r)
-
18
1
U(r)2
U(r)  U(r)2
Reinforces strong (atom-like) features

## Slide 43: S2 Triplet
For reflections h-k, k and h:
(h)  (k) + (h-k)
W. Cochran (1955). Acta. Cryst. 8 473-8.
1
h-k
k
h
= known structure amplitude and phase
= known structure amplitude and unknown phase

## Slide 44: Cochran Distribution (S2): I
Definition:
Consider the product
If the atoms are randomly distributed,
(exponential terms average to zero if m ¹ l)

## Slide 45: Cochran Distribution: II
Consider next
Average is zero
Known
Known Average must be 2np
(
)
-
-
-
+
=
-
-
)
(
)
(
)
(
cos
2
)
(
)
(
)
(
2
2
2
2
h
h
k
k
h)U(h)|
N|U(k)U(k-
-
)|
|U(k-h)U(h)|2
N
|U(k)|
k
U
h
U
h
k
NU
f
f
f

## Slide 46: Cochran Distribution: III
We have a distribution of values. The Central Limit theorem: all distributions tend towards Gaussian. Hence a probability:
P(U(k) - NU(k-h)U(h))
~ Cexp(-|U(k) - NU(k-h)U(h)|2)
~ Cexp(2|U(k)U(k-h)U(h)|cos[f(k)- f(k-h)- f(h)])
Compare to exp(-x2/2s2)
  s2 = 1/4|U(k)U(k-h)U(h)|

## Slide 47: Form of Distribution
Strong Beams
Weak Beams
Note: this is more statistics than the presence of atoms
[f(k)- f(k-h)- f(h)]
Probability
~ 1/2Ö|U(k)U(k-h)U(h)|

## Slide 48: S2 Triplet
For reflections h-k, k and h:
(h)  (k) + (h-k)
W. Cochran (1955). Acta. Cryst. 8 473-8.
1
h-k
k
h
= known structure amplitude and phase
= known structure amplitude and unknown phase

## Slide 49: Example: Si(111) Ö3xÖ3 Au
3f ~ 360n degrees
f=0,120 or 240
f=0 has only 1 atom
120 or 240 have 3
f
f
f
Only one strong reflection
(220)
(1,0)
Other information3 Au
L. D. Marks, et al, Surf. Rev. Lett. 4, 1 (1997).

## Slide 50: Inequalities
|S aibi|2 < S |ai|2 S |bi|2 (Triangle Inequality)
ai = 1/sqrt(N)cos(2pkri) ; bi = 1/sqrt(N)
S aibi = U(k)
S |bi|2 = S 1/N = 1 for N atoms
S |ai|2 = 1/N S cos(2pkri)2
= 1/2N S (1+cos(2p[2k]ri) )
= ½ + U(2k)
Hence U2(k) < ½ +U(2k)/2
If U(k) is large – can set U(2k)

## Slide 51: Quartets
Phase relationships involving 4 terms for weak reflections
  Positive and Negative
  Very useful for x-ray diffraction
  Rarely useful with TEM; dynamical effects can make weak reflections stronger than they should be

## Slide 52: More subtle statistics
Better statistics (Information Theory)
Entropy of a distribution is more fundamental (as is Kullback-Liebler or relative entropy)
Most probable distribution maximizes entropy
S = - ò u(r) ln u(r) dr

## Slide 53: Last step - Refinement
Fit atom positions via:
  Rn =  |Icalc-Iexpt|n/ Iexptn (or Fcalc, Fexpt)
  n =  |Icalc-Iexpt|n/n
  n=1 for Robust Estimation
Should use dynamical Icalc for electrons
R1 < 0.01 for most x-ray structures, < 0.1 currently for TED.
R1~0.5 for random variables

## Slide 54: Crystallographic Direct Methods Structure Triangle
Data
True
Structure
Ideal World
Trial
Structure
Direct Methods Map or Image
Structure Completion (non-trivial)

## Slide 55: Gerchberg-Saxton Algorithm
Optik 35, 237 (1972) Citations > 1500
Paper was rediscovered by Crystallographers in 1990’s

## Slide 56: Algorithm Overview (Gerschberg-Saxton)
Feasible Solution
Fourier Transform
Inverse
Fourier Transform
Impose Fourier space
constraints (S2)
Impose real space
constraints (S1)
Observed Intensities
(assigned phases)
(Global Search)
Recovery
Criterion
YES
NO
Atoms
Intensities

## Slide 57: More: 1970’s Mathematics
C -- Some constraints (e.g. atomicity, probabilities of triplets)
F -- Some function (e.g. a FOM)
Minimize, e.g. Lagrangian
I = F + l C

## Slide 58: 1990’s Mathematics
We have constraints (e.g. atomicity, amplitudes)
  Treat as sets
We are looking for the solution as intersection of several constraint sets
Amplitudes
Atoms
Positivity
Acta Cryst A55, 601 (1999)

## Slide 59: The $64,000 question
A set is convex if any point between two members is also a member
  If all the sets are convex, problem has one solution
  If they are not, there may be more than one local minimum
Amplitude measurements
do not form a convex set
But…there still may only
be one solution.
Unsolved mathematical problem
·
A
C
·
·
|F(k)|=const
B
´

## Slide 60: Multiple non-convex constraints
Overall Convex
Overall Non-Convex
N
U
Consider the two sets “N” and “U”
U
N

## Slide 61: Crystallographic methodology
Overall Non-Convex
Overall Unique
Addition of additional convex constraints tends to give a unique solution
Structure Completion: add additional constraints as the phases become known
U
N

## Slide 62: Orthogonal Projections
Im
Re
0,0
Im
Re
0,0
Estimate
New Value
Modulus Only Part of U(k) known
Project: closest point in set
|U(k)|
|U(k)|
Known

## Slide 63: Successive Projections
Iterate between projections
Other variants possible (see Combettes, Advances in Imaging and Electron Physics 95, 155-270, 1996)
Set of |Uobs(k)|exp(i(k))
Set of U(k) that satisfy
some constraints
Set of all U(k)
Start

## Slide 64: Over-relaxed Projections
Iterate between projections
Overshoot (deliberately)
Converges faster
Sometimes better solutions
Set of |Uobs(k)|exp(i(k))
Set of U(k) that satisfies
atomistic constraints
Set of all U(k)
Start

## Slide 65: Classic Direct Methods
Consider as an iteration
Un(k) un(r)
Constraint Constraint
U’(k) un2(k)
Note the similarities
  Tangent Formula º Orthogonal Projection
  Real space operator, effectively an eigenfunction (fixed point) method

## Slide 66: Multiply-Connected Feasible Set
Probability
Contours
{S1: | F {x}|=|Xe|}
Set with some probability
Three shaded regions common to both sets, 3 unique solutions

## Slide 67: Typical results
Correct
Incorrect
Df = phase error
S|U(k)|{1-cos(Df)}
S|U(k)|

## Slide 68: Types of Constraints
Convex – highly convergent
  Multiple convex constraints are unique
Non-convex – weakly convergent
  Multiple non-convex constraints may not be unique

## Slide 69: More Constraints
Positivity (weak) | Presence of Atoms
Atoms at given positions | Bond Lengths
Least bias (MaxEnt) | Interference A(k)=¦ B(k)+Known(k)¦2
Intensities & errors º c2 | Anti-bumping
Statistics (e.g. S2) | Bond angles
Support for gradient | 
Symmetry | 
Convex
Non-Convex

## Slide 70: Atomistic Constraints
r(r) known (convex if position is known)
Bonding – another atom
Bumping r(r)=0

## Slide 71: Example I: Difference Map
We know all the moduli, |F(k)|
We know part of the structure,
  Fa(k) = |Fa(k)|exp(ifa(k))
Project onto known moduli
  D(k) = exp(ifa(k)){|F(k)obs|-|Fa(k)|}
  Conventional Fourier Difference Map
Other methods (SIM wts) equivalent to further projections.
D
Fa

## Slide 72: Operators as projections
Some operator O, apply to some current estimate (x in real space, X in reciprocal space)
Define a set for the cases where
<O(x)-x> < some number
New estimate obtained by the iteration
xn+1 = O(xn)
N.B., there are some important formal mathematical issues…..

## Slide 73: Example II: Sayre Equation
Use O(x) º ax2 ; a = scaling term
Couple with known moduli as second set
Iteration
  xn+1 = O(xn)= a xn2
  |Xn+1| = |Xobserved|
This is the Sayre equation (and tangent formula)
Iterate

## Slide 74: Example III: Structure Completion
Explanation (pseudo-mathematical) of why structure completion strategies can solve, uniquely, problems when the initial maps are not so good

## Slide 75: Structure Completion
Overall Convex
Add a third set “O”
Addition of additional constraints tends to give a unique solution
Structure Completion: add additional constraints as the atoms become known
Overall Non-Convex
U
N
Consider the two non-convex sets “N” and “U”
Solution

## Slide 76: IV Convex Set for unmeasured |U(h,k,l)|
Phase of U(h,k,l) can be estimated from other reflections
Set of U(h,k,l) with a given phase is convex
Hence |U(h,k,l)| is well
specified and can be
(approximately) recovered
Remember, phase is more
important than amplitude
f
·
·
·
A
B
C

## Slide 77: Support Constraint
Displacements decay as (a+z)exp(-qz) into bulk1
Real space constraint
  r(z)=r(z)w(z) w(z)=1, -L<z<L =0, otherwise
Convex constraint
Has well documented properties
PRB 60, 2771 (1999)
r(z)=0
r(z)¹0
r(z)=0
1Biharmonic expansion of strain field, SS 294, 324 (1993)

## Slide 78: Unmeasured Reflections

## Slide 79: Restoration and Extension
0.3nm Image
+DP
0.05nm Image

## Slide 80: Example V: Diffractive Imaging
True diffraction pattern for small particle model
(Non-Convex Constraint)
+
= ?
Convex Support
Constraint
|(x,y)|=1
|(x,y)|=?

## Slide 81: Example V: Diffractive imaging
Constraint: part of real-space x is zero
Convex constraint
Iteration
  x = 0, part of map
  |X| = |Xobserved|
Iterate

## Slide 82
The flow chart of hybrid input and output algorithm for iterative phase retrieval (after Millane and Stroud, 1997).
Calculate real-space constrained image Cn
Apply Equation
Calculate amplitudes and phases; replace with experimental amplitudes
Inverse Fourier Transform
Forward Fourier Transform
fn
Cn
gn
gn+1
Gn
G’n
The Algorithm
Charge flipping
(Wu and Spence)

## Slide 83
HIO-W
HIO
HIO
HIO
HIO
ER-W
ER
ER
ER
ER
HIO
ER-Error Reduction
HIO-Hybrid Input Output
W-Whole Pattern
Convergence and the Missing Central Beam
Missing central beam from IP saturation
Use low mag. TEM image
Reconstruction start with the whole pattern
Finish with as recorded diffraction pattern

## Slide 84: Phase Recovery for a Small Particle
Reconstructed exit wave after 3000 iterations
True real space exit wave for small particle model

## Slide 85: Electron Nanoprobe formation
Lower Objective
Specimen
Condenser Lens III
Back Focal Plane
10 mm aperture -> 50 nm beam
M = 1/200

## Slide 86
Coherence length > 15 nm
Convergence angle <0.2 mrad

## Slide 87
BL29XUL, SPring-8
Coherent Diffraction Pattern
Coherent X-rays
Sample
Unstained Human Chromosome
Fourier Transform
Phase Retrieval
Coherent X-ray Diffraction
Y. Nishino, Y. Takahashi, N. Imamoto, T. Ishikawa, and K. Maeshima, submitted (2008).
Sample Image
Reconstruction
without the aid of Lenses
Structure Factor
Differential Cross Section
r (r) : Electron Density Distribution

## Slide 88: From 2D to 3D
-60º
-30º
30º
60º
exposure time at each incident angle: 2700 s
Coherent diffraction measurement at 38 incident angles
from -70º to 70º at 2.5º intervals at the minimum
normalize the diffraction data by using
the total number of electrons in the ２D reconstruction
use interpolation to obtain diffraction intensity in each voxel
image reconstruction using 3D Fourier transformation
J. Miao, T. Ishikawa, B. Johnson, E.H. Anderson,
B. Lai & K.O. Hodgson, PRL 89, 088303 (2002)

## Slide 89: Reconstructed Si structure
Nano structures can be reconstructed with atomic resolution by electron diffractive imaging using SAND
SAND pattern
200 spot
・ Intensity ratio of 200 and the direct spots → thickness : 4 ～ 8 nm
direct spot
amplitude
phase
Multi-slice simulated wave fields
reconstructed wave field
0.136 nm
amplitude
・ Dumbbell structure with the separation of 0.136 nm is resolved clearly → We succeeded in reconstructing dumbbell structure in silicon
・ Lattice fringes can be seen, but dumbbell structure is not reconstructed
phase
4nm
6nm
8nm
amp
phase

## Slide 90: Compressive Sensing
From: An Introduction to Compressive Sensing, Olga V. Holtz, http://www.eecs.berkeley.edu/~oholtz/Talks/CS.pdf

## Slide 91: Some notation
L0, L1, L2 metrics
L2 is Least Squares
L1 is a Robust measure
L0 is the number which are > 0

## Slide 92: Robust Statistics & Metrics
L2 is commonly used, but can weight outliers too much. L1 is one version of a Robust Metric
From Numerical Recipes in Fortran 77: The Art of Scientific Computing (ISBN 0-521-43064-x)

## Slide 93: L0 minimization
From: An Introduction to Compressive Sensing, Olga V. Holtz, http://www.eecs.berkeley.edu/~oholtz/Talks/CS.pdf

## Slide 94: L1 minimization
From: An Introduction to Compressive Sensing, Olga V. Holtz, http://www.eecs.berkeley.edu/~oholtz/Talks/CS.pdf

## Slide 95: L1 solves the L0 problem sometimes
From: An Introduction to Compressive Sensing, Olga V. Holtz, http://www.eecs.berkeley.edu/~oholtz/Talks/CS.pdf

## Slide 96: Application for structures
Charge Flipping (Acta Cryst. A 60, 134–141, 2004)
Iterative hard thresholding for compressed sensing (Appl. Comput. Harmon. Anal. 27 (2009) 265–27)
Iterate, setting small values to zero and/or truncate to zero

## Slide 97: Traditional Implementation
Chose phases to define origin
Guess phases for some reflections
Generate from these phases for others and improved phases for initial set
Test consistency of predicted amplitudes and phases
Iterate, so long as consistency is improving
Note: permuting phases has lower dimensions than permuting atom positions

## Slide 98: First Step: Origin Definition
Not all phases are unknown
  Translating the crystal has no physical significance
  Can therefore fix an origin for the crystal – equivalent to fixing certain reflections
  Relevant for crystallographic phase (not absolute phase of wavefunction which is not important)

## Slide 99: Symmetry
Best if determined a-priori
  CBED
  HREM (maybe)
  PED
  Spot Pattern (can be tricky)
Otherwise has to be assumed (may need to try different ones)

## Slide 102: Origin Definition c2mm
1
2
3
4
Mirror Planes

## Slide 103: Origin Definition c2mm
1
2
3
4
(11) Beam Defined
Origin Definition c2mm

## Slide 104: Origin Definition p2mm
1
2
3
4
(11) & (10) Beam Defined
Origin Definition c2mm

## Slide 105: General Formalism as dual
Initial r(r)
Project onto “Real Space Constraint” r2(r)
FFT
Project amplitudes onto Observed
FFT

## Slide 106: In Reciprocal Space: Tangent Formula
If U(r) = U(r)2 = U'( r)
Important part is the phase
U(u) = |U(u)|exp(i); we know |U(u)| but not 
exp(i) = exp(i'); Tan() = Tan(')
Replace old by new one

## Slide 107: Last step - Refinement
Fit atom positions via:
  Rn =  |Icalc-Iexpt|n/ Iexptn (or Fcalc, Fexpt)
  n =  |Icalc-Iexpt|n/n
  n=1 for Robust Estimation
Should use dynamical Icalc for electrons
R1 < 0.01 for most x-ray structures, < 0.1 currently for TED.
R1~0.5 for random variables

## Slide 108: Gerchberg-Saxton Algorithm
Optik 35, 237 (1972) Citations > 1500
Paper was rediscovered by Crystallographers in 1990’s

## Slide 109: Algorithm Overview (Gerschberg-Saxton)
Feasible Solution
Fourier Transform
Inverse
Fourier Transform
Impose Fourier space
constraints (S2)
Impose real space
constraints (S1)
Observed Intensities
(assigned phases)
(Global Search)
Recovery
Criterion
YES
NO
Atoms
Intensities

## Slide 110: When does it work?
Kinematical Diffraction (surfaces)
1s-Channelling
Intensity ordering (PED)
L. D. Marks, W. Sinkler, Sufficient conditions for direct methods with swift electrons. Microsc. Microanal. 9, 399 (2003).

## Slide 111: TED: Si (111) 7x7
Chart: Average
 | 150 | 14150
 | -150 | 13850
Errors independent of intensity (this data set)
Method: Merge data for 6-20 different exposures to obtain accuracies of ~1% with statistical significance
Cross-Correllation Method
P. Xu, et al. Ultramicroscopy 53, 15 (1994).

## Slide 112: 1000 °C in flowing O2
DP’s from Arun Subramanian
_
(110)
(001)
1x1
112
3
1
Notes: Point out which spots are bulk

## Slide 113: Direct Methods Solution
113

## Slide 114: Atomic Positions Refined
114
Notes: 5 Ti 4+ = 20+
13 O 20 = 26-
Total 6-

## Slide 115: SrTiO3 (110) 3x1
TiO2 overall surface stoichiometry
  Ti5O7 atop O2 termination
  Ti5O13 atop SrTiO termination
Surface composed of corner sharing TiO4 tetrahedra
  Arranged in rings of 6 or 8 tetrahedra
  4 corner share with bulk octahedra
  1 edge shares with bulk octahedron
Enterkin et. al., Nature Materials, 2010
Blue polyhedra are surface polyhedra, gold are bulk octahedra, orange spheres Sr, blue spheres Ti, red spheres O

## Slide 116: When does it work?
Kinematical Diffraction (surfaces)
1s-Channelling
Intensity ordering (PED)
L. D. Marks, W. Sinkler, Sufficient conditions for direct methods with swift electrons. Microsc. Microanal. 9, 399 (2003).

## Slide 117: Method
Conventional HREM Image
Nanoprobe
Diffraction Data
FFT
Initial
Phases
W. Sinkler et al. Acta Crystallogr. Sect. A 54, 591 (1998)

## Slide 118: Channeling Approximation
e-
d
2-D Eigenvalue
Talks later by Van Dyck and Chukhovskii will explain more details
S0 distribution is statistically kinematical
Chart: (a)
F. N. Chukhovskii, et al Acta Cryst A 57, 231 (2001)

## Slide 119
Calculated Wave
|y(r)-1| at 113 A thickness
|y(r)-1| at 202 A thickness

## Slide 120
O sites in (Ga,In)2SnO5 determined using
direct phasing of TED data.

## Slide 121: When does it work?
Kinematical Diffraction (surfaces)
1s-Channelling
Intensity ordering (PED)
L. D. Marks, W. Sinkler, Sufficient conditions for direct methods with swift electrons. Microsc. Microanal. 9, 399 (2003).

## Slide 122: Precession Electron Diffraction
Quasi-Kinematical Data
Averaging over angle/phase (and thickness) damps dynamical contributions
Intensities are close to monatomic with structure factors (statistically)

## Slide 123: (Ga,In)2SnO4 precession data: Direct methods solution
DRmean < 4*10-2 Å
(Sinkler, et al. J. Solid State Chem, 1998).
(Own, Sinkler, & Marks, submitted.)
(Real Space)
 | DR (Å)
Sn1 | 0.00E+00
Sn2 | 0.00E+00
Sn3 | 6.55E-03
In/Ga1 | 5.17E-02
In/Ga2 | 2.37E-03
Ga1 | 6.85E-02
Ga2 | 1.22E-01
Displacement (Rneutron – Rprecession):

## Slide 124: Conclusion
The “Phase Problem” with electrons is no longer really a problem….assuming ideal data of course
Many technique work most of the time
Few techniques work all the time
Some unresolved issues (proper dynamical refinement)
Rember that we are solving an inversion problem, and these are susceptible to ill-conditioning

## Slide 125: Four basic elements are required to solve a recovery problem
1. A data formation model
  Imaging/Diffraction/Measurement
2. A priori information
The presence of atoms or similar
3. A recovery criterion:
  A numerical test of Goodness-of-Fit
4. A solution method.
  Mathematical details
Patrick Combettes, (1996). Adv. Imag. Elec. Phys. 95, 155

## Slide 126: Questions ?