## Slide 1: Nanoparticles: from thermodynamics and shape to plasmonics and catalysis
Subtitle
Something old, something new, a lot borrowed, a lot purple
L. D. Marks
Astor Lecture
www.numis.northwestern.edu/Astor_Nanoparticles.pptx

## Slide 2: Acknowledgements 1
Phase 1: 1978-1994
  E. Yoffe, A. Howie, D. J. Smith, J. M. Cowley, J. Dundurs
  P. M. Ajayan, D. Iyer

## Slide 3: Acknowledgements 2
Phase 2: 2008-
K. R. Poeppelmeier R. Van Duyne
J. Enterkin E. Ringe B. Peng D. Alpay S. Patala
Materials Research Science & Engineering Center
Northwestern University
Notes: 3

## Slide 4: Small can be beautiful
Pro’s
  Nanoplasmonics
  Nanoparticles for catalysis
  Sensing
  Drug delivery
  …
Image Source:
John Stringer
Electric Power Research Institute
Notes: 4

## Slide 5: Nanosized Gold
www.notredamedeparis.fr
L. Liz-Marzan, Mater. Today 7, 21 (2004)
Notes: 5

## Slide 6: Single Silver Nanocube LSPR/TEM/FDTD
Y. Wang et al, Ultramicroscopy 2009, 109, 1110-1113.
Notes: 6

## Slide 7: FDTD Results: Effect of Size and Corner Rounding in Ag Cubes
J. M. McMahon, et al, JPCC, 113, 2731 (2009)
Effect of size
Effect of corner rounding
Notes: 7

## Slide 8: Reasonable agreement
8
FDTD
L. J. Sherry, et al, Nano Lett., 5, 2034 (2005); J. M. McMahon, et al, JPCC, 113, 2731 (2009)
40 nm
(1) Distal peak, quadrupolar:
Sharp, high energy, EF away from substrate
(2) Proximal peak, dipolar:
Broader, EF extends into the substrate
1
2
Oleic Acid Surfactant
Notes: 8

## Slide 9: Effect of Size and Substrate, Ag Nanocubes
Proximal
Distal
0.23 eV
Proximal
0.05 eV
Distal
Distal peak  Slope = -4.2(0.55) meV/nm
Proximal peak  Slope = -8.9 (0.5) meV/nm
E. Ringe, et al, JPCC, 114, 12511 (2010)
Notes: 9

## Slide 10: Shape Independent Result
Slope = -2.4(6) meV/nm
Slope = -3.02(5)
Slope = -3.3(2)
Slope = -3.22(9)
Slope = -3.06(4)
E. Ringe, M. R. Langille, J. Zhang, J. Huang, C. A. Mirkin, R. P. Van Duyne, L. D. Marks, J. Phys. Chem. Lett. (2012) 3, 1479
Plasmon Length

## Slide 11: Need Controlled Nanoplasmonics Toolbox
Modeling
Thermodynamic
Kinetic

## Slide 12: Small can be ugly
Con’s
  Toxic
  Wear Debris
Hip Implant
Liao et al., Science 334, 1687 (2011)
Notes: 12
12

## Slide 13: Wear-Mediated Osteolysis
osteoblast
osteoclast/ polymorphonuclear giant cell
http://academic.brooklyn.cuny.edu/biology/bio4fv/page/aviruses/cellular-immune.html
Archibeck, MJ; Jacobs, JJ; Roebuck, KA; Glant, TT. Journal of Bone & Joint Surg, 2000
wear particles
osteolysis
opsonization
phagocytosis
disrupted balance between osteoclasts/PMNs and osteoblasts:
osteoclasts ↑, osteoblasts ↓

## Slide 14: Typical cartoons/visuals used in the literature
Mg3(VO4)2 Mg3V2O6 + 2Obulk
O
Mg
Mg
V
O
O
O
O
O
Mg
Mg
V
O
O
surface
bulk
alkane + Olattice olefin + water
(Reactants) (Products)
O=O
O2-
2e-

## Slide 15: Nanoparticle publications/year

## Slide 16: Overview
Some basics that everyone should know
  Wulff, Winterbottom and friends
Some basics that most do not know or get wrong
  The artifact of some particle size effects
  There are two Wulff constructions
Some new basics
  Segregation in nanoparticles and with strain
A little bit about applications for catalysis

## Slide 17: Basics: Continuum, not so simple
The total energy of an ordered, crystalline nanoparticle can be written as
The ni are positive integers represent the number of atoms along particular directions. Which term is “bulk”, which term is “surface” ?

## Slide 18: Counting Effects
Number of Atoms
= n(n+1)/2
Not n2 dependence
n

## Slide 19: Wulff shape apparently size dependent
Particle-Size Effects on Wulff Constructions. Marks, L.D., Surface Science, 1985. 150(2), 358
Surface Facetting in Small Ceramic Particle. Bonevich, J.E., Proc 47th Ann EMSA, 1989, 258.

## Slide 20: What is the size?
Crystallographic Size
Chemisorption Size
C=O
Thermodynamic Size
V = constant*N

## Slide 21: Care needed
Based on, but not the same as Hamilton, Phys. Rev. B, 2006. 73: 125447, see also Cleveland and Landman JCP, 1991. 94(11), 7376
Simplest approach, define distances such that V(h) = Nvatom
Introduces a non-linear relationship between h & N
Adds some minor corrections
Equimolar Gibbs surface using Wigner-Seitz cells

## Slide 22: Lengths matter
Hamilton, Phys. Rev. B, 2006. 73: 125447, see also Cleveland and Landman JCP, 1991. 94(11), 7376

## Slide 23: Simplification
Bulk Surface Edge Corner
Rewrite as
WD Strain Energy Density
Dimensionless shape term
Surface Stress Contribution

## Slide 24: Weighted Mean Curvature
With Es total surface energy:
=
=
Equilibrium
;
;
The same as Wulff construction (Lagrangian)
For an alloy, , each component j
e.g. Taylor, J.E., Acta Met., 1992. 40(7): p. 1475-1485.

## Slide 25: Geometric interpretation
hi
ri
{ar1+b} /{cri2+dri+e}
 /ri
Nominal equivalent of Gibbs-Thompson term, but for a faceted surface. Suggests that corners are rarely sharp, observed experimentally
Alpay, D., L. Peng, and L.D. Marks, The Journal of Physical Chemistry C, 2015. 119(36), 21018-21023.

## Slide 26: Validation of WMC from DFT
Alpay, D., L. Peng, and L.D. Marks, The Journal of Physical Chemistry C, 2015. 119(36), 21018-21023.

## Slide 27: Surface Energy & Stress
Surface (Free) Energy γ
  Define as energy to create new fully relaxed surface
Surface Stress
  Derivative with strain
Shuttleworth equation is not correct with definitions per atom

## Slide 28: Anatase TiO2 showing an expansion Ahmad, M.I. and S.S. Bhattacharya, Applied Physics Letters, 2009. 95(19), 191906.
(a)
(b)
Relative decrease in lattice parameter in Ag3Sn
N., M. Knipper, J. Parisi, T. Plaggenborg, and J. Kolny-Olesiak, Journal of Physical Chemistry C, 2015. 119(25), 14450-14454.
Surface Stress leads to lattice changes

## Slide 29: Basics: Continuum, simple
The total energy of an ordered, crystalline nanoparticle can be written as
Bulk Surface Edge Corner
Thermodynamic shape for reasonable sizes minimizes E at a fixed volume
Find the shape that optimizes the surface energy

## Slide 30: Wulff Construction
Minimize surface energy for fixed volume
Max Von Laue
G. Z. Wulff, Kristallogr. Mineral 34, 4490 (1901); M. Z. Von Laue, Kristallogr. 105, 124 (1943); A. Z. Dinghas, A. Z. Kristallogr. 105, 304 (1944)

## Slide 31: Example: SrTiO3
10nm
Crosby, L., J. Enterkin, F. Rabuffetti, K. Poeppelmeier, and L. Marks, Surface Science, 2015. 632, L22-L25
Notes: 31

## Slide 32: Chemisorption Dependent
Cu Bi-saturated Cu
Curtesy Paul Wynblatt

## Slide 33: Winterbottom Construction
gInt
Include the effect of a nanoparticle sitting on a substrate

## Slide 34: Wulff & Winterbottom
34
Increasing γint
Increasing γsub
Increasing γPt
J. A. Enterkin, K. R. Poeppelmeier, L. D. Marks, Nano Lett. 11, 993 (2011); G. Z. Wulff, Kristallogr. Mineral 34, 4490 (1901);
W. L. Winterbottom, Acta Metallurgica 15, 303 (1967)
45° rotation around [100]
Projection down [010]
Projection down [110]
γ100
100
001
γ111
γ111
γ111
001
110
γInt – γSub = 0
γInt – γSub ≤ -γPt
-γPt < γInt – γSub < 0
γInt – γSub = γPt
0 < γInt – γSub < γPt
51° rotation around [011]

## Slide 35: Depends upon environment
As prepared (oxidized) Reduced (after WGS)
Lin, Y., Z. Wu, J. Wen, K. Ding, X. Yang, K.R. Poeppelmeier, and L.D. Marks, Nano Lett, 2015. 15(8), 5375-5381

## Slide 36: Caveat: assumes flat substrate
Connects to SMSI
Ajayan, P.M. and L.D. Marks, Nature, 1989. 338(6211), 139

## Slide 37: Continuing, beyond single crystals
Reduce surface energy, at the cost of strain energy
Decahedral MTP Icosahedral MTP

## Slide 38: Distorted tetrahedral units
S. Ogawa & S. Ino, J. Vac. Sci., Tech. 6, 527 (1969).

## Slide 39: But…Dh is not so simple
L. D. Marks,. Philos. Mag. A. 49, 81 (1984).

## Slide 40: Modified Wulff Construction
gtwin/2
Include the effect of a nanoparticle with a twin

## Slide 41: LTPs

## Slide 42: Modified Wulff Construction
L. D. Marks,. Philos. Mag. A. 49, 81 (1984).

## Slide 43: Modified Wulff Construction
L. D. Marks,. Philos. Mag. A. 49, 81 (1984).

## Slide 44: Dh & Ic segments

## Slide 45: Modified Wulff Construction for Twinned Particles
L. D. Marks, J. Cryst. Growth 1983, 61, 556-566
Lamellar Twinned Particles
2 or more segments
1 boundaries/segment (caps)
2 boundaries/segment (middle)
Decahedral
Multiply Twinned Particle
5 segments
2 boundaries/segment
Icosahedral
Multiply Twinned Particle
20 segments
3 boundaries/segment
Notes: 45

## Slide 46: Shapes for Dh reported in 19th century – “Fivelings”
From H. Hofmeister, Z Krist 224 (2009) 528

## Slide 47: Different Cases
E. Ringe, R.P. Van Duyne, L. D. Marks, Journal of Physical Chemistry C, 2013. 117, 15859

## Slide 48: Different Shapes for Ic as well
Images courtesy of M. Yacaman
{111} only
{110} only
{111} + {110}
N.B., no {100} in an Ic, see L. D. Marks, Philos. Mag. A. 49, 81 (1984)

## Slide 49: Surfaces depend upon environment
“5x1” (001) reconstruction on Au Dh, Image courtesy of Gilberto Casillas-Garcia, UTSA

## Slide 50: MTP Energetics
Three Terms
  Strain, fcc units do not fit together without it
  Difference in total surface free energy
  Difference in total surface stress terms
  N.B., twin boundary energy negligable

## Slide 51: Strain: Volterra Disclination
Von Mises stress distribution (a)
R. de Wit, Journal of Physics C, 1972, 5, 529
A. Howie and L. D. Marks, Phil Mag 1984. 49(1), 95-109.
Patala, S., L.D. Marks, and M.O. de la Cruz, Journal of Physical Chemistry C, 2013. 117(3), 1485
S. Ogawa & S. Ino, J. Vac. Sci. Tech. 6, 527 (1969).

## Slide 52: MTPs have less of the Wulff shape
Twin boundaries restrict which surfaces are exposed
L. D. Marks,. Philos. Mag. A. 49, 81 (1984).
Segment for Dh

## Slide 53: Energy Balance
Three competing terms
  Gain in surface energy (MTPs more {111})
  Cost to strain the particle
  Energy change due to expansion at surface, surface stress term (heavily environment dependent)
Chart: 
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20
Sc | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5
Dh | 3.15 | 3.3 | 3.45 | 3.6 | 3.75 | 3.9 | 4.05 | 4.2 | 4.35 | 4.5 | 4.65 | 4.8 | 4.95 | 5.1 | 5.25 | 5.4 | 5.55 | 5.7 | 5.85 | 6
Ic | 2.3 | 2.6 | 2.9 | 3.2 | 3.5 | 3.8 | 4.1 | 4.4 | 4.7 | 5 | 5.3 | 5.6 | 5.9 | 6.2 | 6.5 | 6.8 | 7.1 | 7.4 | 7.7 | 8
A. Howie and L. D. Marks, Phil Mag 1984. 49(1), 95-109.
Ic Dh Sc

## Slide 54: Energetics
Icosahedra
Quasi-spherical shape.
Close-packed surface but
large internal strain.
Favourable at small sizes
Decahedra
Intermediate behaviour.
Favourable at
Intermediate sizes
Polyhedra
Non-spherical shape
No internal strain.
Favourable at large sizes
Courtesy Riccardo Ferrando

## Slide 55: Growth
Complex, can be templated (i.e. large from small) or there can be changes
K. Yagi et al, Journal of Crystal Growth 28 (1975) 117

## Slide 56: Growth
K. Yagi et al, Journal of Crystal Growth 28 (1975) 117
L. D. Marks, Journal of Crystal Growth 61(1983) 556
Asymm Dh Dh Dh Ic

## Slide 57: Structural Fluctuations (Iijima)
P. M. Ajayan, L. D. Marks,. 24-6, 229 (1990)

## Slide 58: A simple physical concept
Courtesy of Stephen Berry
The potential surface, very schematically: solid in the deep, narrow well, liquid in the high rolling plain:

## Slide 59: Quasimelting
b
b
J. Dundurs, L. D. Marks, P. M. Ajayan,. Philos. Mag. A. 57, 605 (1988)

## Slide 60: Phase Diagram (1990 vintage)
P. M. Ajayan, L. D. Marks. Phase Transit. 24-6, 229 (1990)

## Slide 61: Morphological Transitions (Angus Kirkland)
Room temp
300°C
400°C
FCC
Decahedral
RT
400°C
RT
Icosahedral
Decahedral
In-situ Heating
RT
400°C
RT
Decahedral
Decahedral
5.5nm size
7.2nm size
10.4nm size
Ultramicroscopy, 110 (2010) 506
ACS Nano, 3 (2009) 1431
Solid – Solid Transition below Tm
As Synthesised Particles not in Thermodynamic Ground State

## Slide 62: The Two Wulff Constructions
Just to make life more fun
  Is every Wulff shape thermodynamic
  No, and probably the original paper was not

## Slide 63: Thermodynamic Wulff Construction
γ = surface free energy
n = crystallographic face (hkl)
h(n) = surface normal
Λ(c) = Wulff constant (accounts for volume)
γ100
γ111
001
110
100
001
γ111
100 << 111 100 ~
G. Z. Wulff, Kristallogr. Mineral. 34, 449 (1901)
Notes: 63

## Slide 64: Kinetic Wulff Construction
v= growth velocity
n = crystallographic face (hkl)
h(n) = surface normal
Λ(c) = Wulff constant (accounts for volume)
γ100
γ111
001
110
100
001
γ111
Frank, F. C. In Growth and Perfection of Crystals; Doremus, R. H., Roberts, B. W., Tumbull, D., Eds.; Wiley (1958)
Notes: 64

## Slide 65: Schematic for growth
Nucleation barrier for terrace

## Slide 66: Kinetic v Thermodynamic Wulff
i depends upon
Chemisorption
Surface Composition
Bulk Composition
Surface Segregation
vi depends upon
Rate limiting step (diffusion/nucleation)
Transition state (e.g. desorption of surfactants)
, i.e. local chemical potential

## Slide 67: Origin of twin enhancement term
Atoms added at a twin have a higher co-ordination number than on a flat surface
Additional energy makes nucleation easier

## Slide 68
Kinetic Wulff Construction for Twinned Particles
Kinetic Wulff: Growth Velocity
Twinned Wulff: Assemble Segments
+ Growth enhancement
Frank, F. C. In Growth and Perfection of Crystals; Doremus, R. H., Roberts, B. W., Tumbull, D., Eds.; Wiley (1958)
L. D. Marks, J. Cryst. Growth 61, 556 (1983) ;E. Ringe, R.P. Van Duyne, L. D. Marks, Journal of Physical Chemistry C, 2013. 117, 15859
Re-entrant surface growth enhancement
Disclination/twin boundary growth enhancement
5X
=

## Slide 69
Re-entrant growth
Disclination + re-entrant
100 nm
B. Petrobon, M. McEachran, V. Kitaev, ACS Nano 2009, 3, 21-26
Modified Kinetic Wulff Construction:
Shape of Dh Structures
111
100
γ111/ γ100 = 3/2
Re-entrant + Stable 111
Notes: 69

## Slide 70: Diamond for different conditions
1.3 1.4 1.7 1.9 2.5
J. Bühler, Y. Prior, J Cryst Growth 209 (2000) 779

## Slide 71
Modified Kinetic Wulff Construction:
Shape of {111} – Dominated Monotwin Structures
Twin growth enhancement
Twin + re-entrant growth enhancement
Re-entrant surface growth enhancement
Notes: 71

## Slide 72: Alloy Wulff Construction
Alloy Wulff has an extra degree of freedom: surface composition
Use available/measurable parameters (surface/bulk energies) to produce a predictive model
Result of energy minimization: size-dependant balance between
  Surface energy
  Starvation energy
γ100
γ111
001
110
100
001
γ111
E. Ringe, R.P. Van Duyne, L. D. Marks, Nano Lett. 11, 3399 (2011)
Notes: 72

## Slide 73
Alloy Wulff Construction:
Minimization of Energy via Lagrangian Multipliers
γ = surface free energy
n = crystallographic face
CSi = surface concentration of element i
CVi = bulk concentration
G = bulk free energy
Λ = Wulff constant (accounts for volume)
hn = surface normal
Conventional Wulff
Alloy Wulff
γ = surface free energy
n = crystallographic face
hn = surface normal
Λc = Wulff constant (accounts for volume)
Size Independent
Size Dependent: Starvation
h(100)
h(110)

## Slide 74: Comparison of Methods
Conventional Wulff
X Segregation
X Starvation
Infinite Reservoir
Segregation
X Starvation
Alloy Wulff
Segregation
Starvation
Surface
Bulk

## Slide 75
3 Regimes in CuAu Alloy Wulff Construction
1 2 3
1 2 3
1: De-alloying 2: Bulk/surface equilibrium 3: Monolayer formation
γAu < γCu
Notes: 75

## Slide 76: Strain: Disclination
Von Mises stress distribution (a) Top-view along the disclination axis and (b) with a plane-cut (perpendicular to the disclination axis) through the geometric center of particle
Patala, S., L.D. Marks, and M.O. de la Cruz, Journal of Physical Chemistry C, 2013. 117(3), 1485

## Slide 77: Strain-driven segregation?
Distribution of point defects around a dislocation line,
Distribution Au atoms
Problem Maps to Cottrell Cloud Problem
Peng, L.X., R.P. Van Duyne, and L.D. Marks, Journal of Physical Chemistry Letters, 2015. 6(10), 1930-1934

## Slide 78: Segregation at different Temperatures
No significant segregation when temperature is high
Peng, L.X., R.P. Van Duyne, and L.D. Marks, Journal of Physical Chemistry Letters, 2015. 6(10), 1930-1934

## Slide 79: Experimental Data Needed
Shape
Surface/bulk Composition
H. E, P. D. Nellist, S. Lozano-Perez, D. Ozkaya, J. Phys. Conf. Series 241, 012067 (2010)
F. Krumeich, S. Marx, A. Baiker, R. Nesper, Z. Anorg. Allg. Chem. 637, 875 (2011)
Notes: 79

## Slide 80: Can we exploit these ideas
80
NO on Pt Masel, 1983
Winterbottom construction, different exposed facets
Substrate
J. A. Enterkin, K. R. Poeppelmeier, L. D. Marks, Nano Lett. 11, 993 (2011);

## Slide 81: Propane Oxidation
Pt/SrTiO3 epitaxy stabilizes metallic Pt
  For particle of radius R DG=DGOx+3DgInt/2R
  More reactive Pt/PtOx core/shell structure in oxidizing conditions
  Flux of reactants also different for different surfaces
J. A. Enterkin, W. Setthapun, J. W. Elam, S. T. Christensen, F. A. Rabufetti, L. D. Marks, P. C. Stair, K. R. Poeppelmeier, C. L. Marshall,
ACS Catalysis 1, 629 (2011)
Chart: Temperature (°C)
| 25 | 50 | 75 | 100 | 125 | 150 | 175 | 200 | 225 | 250 | 275 | 300 | 325 | 350 | 375 | 400 | 425 | 450 | 475 | 500 | 525 | 550
Nanocubes Cycle 1 | 0 | 0 | 0 | 0 | 0 | 0.59132 | 1.9706 | 6.2393 | 21.3693 | 58.6607 | 75.2656 | 85.3478 | 91.2173 | 95.6237 | 97.8908 | 99.2388 | 100.0211 | 100.1789 | 99.9559 | 99.9618 | 100.5067 | 100.2013
Nanocubes Cycle 2 | 0 | 0 | 0 | 0 | 0.12506 | 0.66742 | 2.5068 | 7.8454 | 37.0971 | 62.0384 | 75.394 | 84.5059 | 90.0892 | 93.6365 | 96.5822 | 98.4803 | 99.5066 | 100.0231 | 100.2119 | 100.4662 | 100.1684 | 100.5609
Nanocubes Cycle 3 | 0 | 0 | 0 | 0 | 0.23957 | 0.64074 | 2.2422 | 7.3214 | 28.1959 | 56.2254 | 69.1507 | 78.9498 | 85.1363 | 89.8721 | 93.2419 | 95.6559 | 97.3368 | 98.6955 | 99.6002 | 99.7891 | 100.4768 | 100.6423
Nanocubes Cycle 4 | 0 | 0 | 0 | 0 | 0 | 0.56038 | 2.0502 | 7.2643 | 29.3597 | 55.4226 | 69.1758 | 77.9196 | 84.306 | 88.4441 | 91.7451 | 94.3038 | 96.3328 | 97.7205 | 99.0418 | 98.808 | 99.2207 | 99.7945
Powder Cycle 1 | 0 | 0 | 0 | 0 | 0 | 0.31169 | 0.36732 | 0.94058 | 1.8945 | 4.2965 | 8.5154 | 15.3258 | 25.3904 | 36.5296 | 47.3075 | 56.1887
Powder Cycle 2 | 0 | 0 | 0 | 0 | 0 | 0 | 0.53751 | 0.9932 | 2.4026 | 5.0151 | 9.4394 | 16.3008 | 25.3412 | 35.5785 | 45.2132 | 54.9185
Powder Cycle 3 | 0 | 0 | 0 | 0 | 0 | 0.14959 | 0.45555 | 1.1941 | 2.361 | 5.0269 | 9.369 | 16.4134 | 25.8246 | 36.1987 | 46.3036 | 55.8707 | 64.0287 | 70.4759 | 75.8885 | 79.6901 | 82.853 | 85.2465
Powder Cycle 4 | 0 | 0 | 0 | 0 | 0 | 0 | 0.60244 | 1.0792 | 2.3401 | 4.4779 | 8.2964 | 13.4538 | 20.0931 | 27.293 | 34.2376 | 41.3249 | 47.3833 | 53.0104 | 58.7655 | 64.6375 | 70.6224 | 77.0633
Cycle 1 | 1
Cycle 2 | 1
Cycle 3 | 1
Cycle 4 | 1

## Slide 82: Catalysts by design
Oleic Acid
1nm
SrO surface
1nm
TiO2 DL
TiO2
(100)
(100)
SrO
(111)
(100)
(111)
(111)
Chart: CO Oxidation
| 4.4779274611398963 | 4.9754749568220999 | 5.597409326424871 | 6.3970392301998524 | 7.463212435233161 | 8.9558549222797925
Oleic Acid STO | 0.070039 | 0.073993 | 0.083501 | 0.088986 | 0.10942 | 0.11298
Acetic Acid STO | 0.021527 | 0.02352 | 0.024785 | 0.028504 | 0.032837
Acetic Acid

## Slide 83: Summary
While we know at lot from old work (even back to Gibbs)
Care is needed
  Being precise with size matters
Nanoalloys has some new possibilities
Still manye things that are not fully understood

## Slide 84: Questions ?
Research is to see what everybody else has seen, and to think what nobody else has thought Albert Szent-Györgi
www.numis.northwestern.edu/Astor_Nanoparticles.pptx