## Slide 1: Oxide Surfaces: Opening the Pandora’s Box
L. D. Marks
Astor Lecture
Surfaces
DFT
Structure
10 nm
NanoCatalysts
Catalysis
William Waldorf Astor, 1st Viscount Astor

## Slide 2: Acknowledgements
TEM: N. Erdman (JEOL), A. Subramanian (Intel), A. Chiaramonti (NIST), A. Becerra (Dow), J. Enterkin (Philips 66), E. Ringe (Rice), D. Keinzle (Premier International), Y. Lin (TDK), L. Crosby, D. Alpay, L. Peng, L. Lian, P. Koirla
DFT: A. Becerra, J. Enterkin, D. Keinzle, Y. Lin, S. Cook & LDM
Modelling: E. Ringe, L. Peng, S. Cook, P. Koirla, & LDM
STM: R. Shams, B. Russell, Z. Wang
STM Simulations: A. Becerra, Y. Lin & LDM
Synthesis: L. Hu, Y. Lin, C. Wang, L. Crosby, B.-R. Chen
Catalysis: L. Hu, Y. Lin, C. Wang, B.-R. Chen
Collaborators:
K. R. Poeppelmeier (NU), P.C. Stair (NU), M. Bedzyk (NU), R. Van Duyne (NU), P. Blaha (Vienna), M. Castell (Oxford), O. Warschkow (U. Sydney), U Diebold (Vienna), C. Marshall (ANL), S. Overbury (ORNL), J. Ciston (LBNL), L. Allen (Melbourne)

## Slide 3: Motivation
Oxide surfaces are everywhere:
  Everything in this room
  Active catalysts
  Catalytic supports
  Multiferroic Oxides
  Solid Oxide Fuel Cells
  Corrosion products
  Metal implants
  Buildings (cement)
Baha’i Temple, Wilmette, IL

## Slide 4: Looking to the future
Need to better understand oxide surfaces:
Reduce corrosion, ~3% of GDP
Reduce friction, ~ 5% of GDP
Understand why implants fail
Quality control for low-power oxide electronics
Deliberate design of better catalysts
Image Source:
John Stringer
Electric Power Research Institute

## Slide 5: Corrosion Costs ~ 350 Billion $/Yr in the US
Rusted Deck and Ventilation Equipment
Source: www.corrdefense.org
Much of the science of corrosion was developed in the 1980’s or earlier
What is really going on at the atomic scale?
What can 21st Century tools tell us about ways to minimize corrosion?
Tuesday’s Lecture

## Slide 6: Friction
~5% of GDP
30% of power in a new auto engine
http://www.fueleconomy.gov
“…the greatest source of new energy is the energy we waste today.”
Samuel Bodman, U.S. Secretary of Energy, 2008

## Slide 7: ~1/2 Million/Yr in US
In 20 years implants will be grown (and/or printed)
That is not soon enough
Metallic biomedical implants corrode in the human body leading to severe problems
What is going on? How do we improve them? Do different surface oxides matter?
Tuesday’s Lecture

## Slide 8: Oxide Electronics
For oxide electronics to be commercial five-sigma reproducibility will be required
What are the real details, atom-by-atom of oxide MBE growth?
How do we control it, precisely?

## Slide 9: How many phases are there?
One for each material?
One for each material and each interface?
One for each material, each interface and the surface?

## Slide 10: Example
Becerra-Toledo AE, Castell MR, Marks LD. Water adsorption on SrTiO3(001): I. Experimental and simulated STM. Surf Sci. 2012;606(7-8):762-5.
Dehydration

## Slide 11: Better Catalysts, by Design
1nm
TiO2 DL
Control the nanoparticles by epitaxy on oxides
J. A. Enterkin, K. R. Poeppelmeier, L. D. Marks, Nano Lett. 11, 993 (2011)

## Slide 12: ….at an oxide surface
This cartoon is almost certainly far from reality about the surface structure
Mg3(VO4)2 Mg3V2O6 + 2Obulk
O
Mg
Mg
V
O
O
O
O
O
Mg
Mg
V
O
O
surface
bulk
alkane + Olattice olefin + water
(Reactants) (Products)
O=O
O2-
2e-
The activity and selectivity are
closely related to the structures
of the catalyst used.
Mg3V2O8
Mg3V2O6
[011]
[100]
H2 / propane
Typical cartoons/visuals used in the literature

## Slide 13: Broad Vision
Time
Discovery-based
Time
Oxide Surfaces By Design
Adapted From: Paget Donnelly, Nanomaterials By Design, Chemical Industry R&D Roadmap, www.chemicalvision2020.org/downloads/nanochemroadmap_presentation_1-5-04.ppt

## Slide 14
Ti
(110)
Single Crystal
Growth
Crystallography
Direct Methods & DFT
Ti
O
Sr
10 nm
Nanoparticle
Synthesis
Surface
Structure
Catalytic Oxides
Catalytic
Activity
Thermodynamics
Bridge the Materials Gap

## Slide 15: The question
What is the structure of oxide surfaces, what are the building blocks and does it have short-range, long-range or other order/disorder?
Do Pauling’s rules apply to surfaces?

## Slide 16: Pauling’s Rules
The radius ratio rule
The electrostatic valence rule
  Bond Valence Sums & local electroneutrality
Sharing of polyhedron corners, edges and faces
Crystals containing different cations
The rule of parsimony
  The number of building blocks is small

## Slide 17: Key experimental tools
100-300 keV
Both give approximately kinematical data for surfaces
Weak Signals
Electron scattering is substantially stronger than x-ray, better S/N
7 GeV

## Slide 18: First Core Method
Incident 100-300 kV electrons
Collect images or diffraction information
+SXRD, STM, XPS, DFT….
e-

## Slide 19: Sample preparation (an art)
Cut 3mm disc or mount sample
Dimple thin to 10 mm
Thin to < 0.1 mm
  Ion beam (damage)
  Chemical (?)
Anneal damage (carefully!)
Last step similar to making new oxides
  Try a time/temperature: if it works, celebrate
  If it does not, try again…..
  All you need are enough slaves grads/undergrads
Dimple Wheel
Sample

## Slide 20: SrTiO3 (111): Pre-annealing
Sample is under stress, disordered, and non-stoichiometric
(110)
100 nm
diffuse ring
~100 Å
[111]
A. N. Chiaramonti et al., Surf. Sci. 602, 3018 (2008).

## Slide 21: Annealing
In-situ
Ex-situ

## Slide 22: SrTiO3 (111): Annealed
Surfaces are:
  ordered, flat
  covered in large often triangular terraces and step bunches
Reconstructed
Air stable (months)
Reproducible
100 nm
A. N. Chiaramonti et al., Surf. Sci. 602, 3018 (2008).

## Slide 23: Second Core: Solve Structures
Indirect Methods:
“Trial and Error”
Direct Methods:
Using available information
to find solutions

## Slide 24: Second Core: Direct Methods
Not as simple as it looks !
L. D. Marks, W. Sinkler, and E. Landree, Acta Cryst A55, 601 (1999) L. D. Marks, Phys. Rev. B 60, 2771 (1999)
L. D. Marks et al., Surf. Rev. Lett. 5, 1087 (1998).
R. Gerschberg and W. O. Saxton, Optik 35, 237 (1972)

## Slide 25: Third Tool: DFT
GIGO – DFT only refines, it is not a search method
DFT energies can have serious errors for oxides
All DFTs are equal, but some DFTs are more equal than others
Atoms
Paper
DFT Black Box
Apologies to George Orwell

## Slide 26: Perovskite Surfaces (2002)
~43,000 articles on perovskites
  ~21,000 on strontium titanate
637 articles on perovskite surface structures
  571 articles say what reconstruction is present
None provide crystallographic solutions to surface structures
26

## Slide 27: SrTiO3 reconstructions (2015)
(001) | (110) | (111)
2x1 Ö2xÖ2 2x2 c4x2 c6x2 √5x√5 √13x√13 | 3x1 4x1 5x1 6x1 2x4 2x5 | 2x2 3x3 4x4 5x5 6x6 9x9
About 40 different reconstructions reported
15 have been solved
The most complex surfaces of any known material
Previously published
Today
Submitted

## Slide 28: Four examples
Connect TED, DFT, STM (and chemistry); the SrTiO3 (110) surface
What lies beyond order: glass-like tilings (constrained Ising model) on SrTiO3, the Ö13xÖ13 (001) reconstruction
Entropy and disorder, more complex Pott’s model for SrTiO3 (111)
What happens with nanoscale oxides?

## Slide 29: SrTiO3 (110): 900C in O2
40 nm
001
1x1
29
N. Erdman, PhD Thesis, 2002
Dark Field

## Slide 30: 1000 °C in flowing O2
DP’s from Arun Subramanian
_
(110)
(001)
1x1
3
1

## Slide 31: Direct Methods Solution

## Slide 32: Atomic Positions Refined
32

## Slide 33: SrTiO3 (110) 3x1
TiO2 overall surface stoichiometry
  Ti5O7 atop O2 termination
  Ti5O13 atop SrTiO termination
Surface composed of corner sharing TiO4 tetrahedra
  Arranged in rings of 6 or 8 tetrahedra
  4 corner share with bulk octahedra
  1 edge shares with bulk octahedron
Enterkin et. al., Nature Materials, 2010
Blue polyhedra are surface polyhedra, gold are bulk octahedra, orange spheres Sr, blue spheres Ti, red spheres O

## Slide 34: SrTiO3 (110) nx1
3x1
4x1
∞x1
2x1
3x1
4x1
5x1
6x1
Expansion to other nx1 by changing the number of TiO4 surface tetrahedra per ring

## Slide 35: Intergrowths
STM with simulations (DFT)
Enterkin et. al., Nature Materials, 2010
4x1
3x1
3x1
6x1
5x1
6x1
4x1
4x1
5x1

## Slide 36: Bond Valence Sums (BVS)
Development of electronegativity/positivity concepts from work of Pauling and others
Idea is that the valence of an atom is the sum of the individual bond valences surrounding the atom
If BVS is “right”, energy is low; if BVS not right often problems with structure
This is a Bulk concept, used in surface science all the time (e.g. XPS is calibrated against BVS)
BVS & DFT are consistent, as they have to be

## Slide 37: STO (110) Bond Valence Sums
Bond Valence |  | Sr | Half-O2 | ¥x1 | 6x1 | 5x1 | 4x1 | 3x1 | 2x1
Surf | Ti(Sr) | 1.88 | 3.83 | 3.41 | 3.87 | 3.93 | 3.99 | 4.06 | 4.02
Surf | O | 1.49- | 1.94- | 1.21- | 1.88- | 1.95- | 1.99- | 2.05- | 2.07-
Sub-surf | O | 2.61- | 1.88- | 2.07- | 2.02- | 2.04- | 2.05- | 2.05- | 1.94-
Chart: 
| -1 | 0 | 1.3333333333333333
 | 0.88982 | 0 | -0.23755
 | 0.88982 | -0.23755 | -0.29244 | -0.33782 | -0.2011 | 0.44465
Surface Energy
(eV per 1x1 unit)
X: TiO2 at Surface
SrO monolayer
at Surface
TPSSh

## Slide 38: Four examples
Connect TED, DFT, STM (and chemistry); the SrTiO3 (110) surface
What lies beyond order: glass-like tilings (constrained Ising model) on SrTiO3, the Ö13xÖ13 (001) reconstruction
Entropy and disorder, more complex Pott’s model for SrTiO3 (111)
What happens with nanoscale oxides?

## Slide 39: STiO3 (001) Energies
Chart: 
| 0.5 | 1.5 | 1.5 | 1.5 | -0.5
100 | 1.3727 | 1.79 | 1.6977 | 1.4621 | 1.292
 | 1.192 | 1.2727 | 1.3621
 | 1.392 | 1.4727 | 1.5621
SrO
Ö2
2x2
c4x2
TiO2
TiO2 per 1x1
eV/1x1 cell, revTPSSh
For errors, see L. D. Marks et al., Surf. Sci. 603, 2179 (2009) For revTSPP J.P. Perdew, PRL 103, 026403 (2009)

## Slide 40: Common features: 1x1 Base
Building Blocks:
5-fold Ti 6-fold Ti
Top View Side View
Sr (not critical)

## Slide 41: 2x2 Structure
O. Warschkow et al., Surf. Sci. 573, 446 (2004).
Top View Side View

## Slide 42: Ö2xÖ2 R45
O. Warschkow et al., Surf. Sci. 573, 446 (2004).
Top View Side View

## Slide 43: c(4x2)
N. Erdman et al., J. Am. Chem. Soc. 125, 10050 (2003).
Top View Side View

## Slide 44: Constrained Ising Model
1
1
1
1
1
1
1
1
1
1
1
1
= 1
1
1
1
1
1
1
1
Pauling’s 5th rule, parsimony

## Slide 45: STiO3 (001) Energies
Chart: 
| 0.5 | 1.5 | 1.5 | 1.5 | -0.5
100 | 1.3727 | 1.79 | 1.6977 | 1.4621 | 1.292
 | 1.192 | 1.2727 | 1.3621
 | 1.392 | 1.4727 | 1.5621
SrO
Ö2
2x2
c4x2
TiO2
TiO2 per 1x1
eV/1x1 cell, revTPSSh
Intermediate compositions?
For errors, see L. D. Marks et al., Surf. Sci. 603, 2179 (2009) For revTSPP J.P. Perdew, PRL 103, 026403 (2009)

## Slide 46: Ö13xÖ13 R33.7 SrTiO3 (100)
Make a “normal” sample
Buffer-etched then annealed
Changes surface TiO2 excess
D. M. Kienzle, A. E. Becerra-Toledo, and L. D. Marks,
Phys. Rev. Lett. 106, 176102 (2011)

## Slide 47: (001) Ö13xÖ13 Initial Map

## Slide 48: Larger tilings (Ising Model)
Ö13xÖ13
3x3
Ö5xÖ5

## Slide 49: Stable according to DFT
Chart: 
| 0.5 | 1.5 | 1.5 | 1.5 | -0.5 | 1.2692307692307692 | 1.1000000000000001 | 1.3888888888888888
100 | 1.3727 | 1.7778 | 1.7028 | 1.4621 | 1.292 | 1.2389 | 1.3625 | 1.3313
 | 1.192 | 1.1389 | 1.3621
 | 1.392 | 1.3389 | 1.5621
SrO
Ö2
2x2
c4x2
TiO2
Ö13
Ö5
3x3
TiO2 per 1x1
eV/1x1 cell, revTPSSh
Glasses
D. M. Kienzle, A. E. Becerra-Toledo, and L. D. Marks, PRL. 106, 176102 (2011)

## Slide 50: Four examples
Connect TED, DFT, STM (and chemistry); the SrTiO3 (110) surface
What lies beyond order: glass-like tilings (constrained Ising model) on SrTiO3, the Ö13xÖ13 (001) reconstruction
Entropy and disorder, more complex Pott’s model for SrTiO3 (111)
What happens with nanoscale oxides?

## Slide 51: In This House We Obey The Laws of Thermodynamics
Homer Simpson
aka Free Energy
Enthalpy and Entropy

## Slide 52: SrTiO3 (111)
Complex series of nxn reconstructions, 2<n<6
Similar to other surfaces or not?
100 nm
L. D. Marks, A. N. Chiaramonti1, S. U. Rahman and M. R. Castell, PRL, in press

## Slide 53: Is it just enthalpy that matters?
At elevated temperatures configurational entropy can dominate for Potts/Ising models
In an ideal solution model with variable TiO2 excess at the surface,
ci is the fraction of each surface phase, Gi the free energy per 1×1 unit cell, ni the number of cells in the surface unit cell, fi the TiO2 excess per 1×1 unit cell and  the TiO2 surface chemical potential.

## Slide 54: 3x3 & 4x4 ordered
3x3
4x4
Green TiO4, similar to (110)
Purple, TiO5, similar to (001)
Brown TiO6
Similarities to both (110) & (001)
TED

## Slide 55: 2x2 more complex
More than one 2x2 structure

## Slide 56: Convex Hull
TiO2 excess per 1×1 unit cell
eV

## Slide 57
Chart: 
| -0.5 | 0.5 | 1.5 | 1.5 | 1.75 | 1.75 | 1.8333333333333333 | 1.875 | 1.875 | 2 | 2 | 2 | 2 | 3 | 2.5 | 2
 | 3.437 | 2.9091 | 2.7881 | 2.7139 | 2.8089 | 2.7925 | 2.8773 | 2.9592 | 2.9317 | 3.0209 | 3.0318 | 3.0575 | 3.0105 | 4.0338 | 3.2441 | 3.0953

## Slide 58: Configurational disorder, Potts prediction
3 dimer orientations of 2x2, rotational glass
3x3 (crosses) embedded
Result is general

## Slide 59: Four examples
Connect TED, DFT, STM (and chemistry); the SrTiO3 (110) surface
What lies beyond order: glass-like tilings (constrained Ising model) on SrTiO3, the Ö13xÖ13 (001) reconstruction
Entropy and disorder, more complex Pott’s model for SrTiO3 (111)
What happens with nanoscale oxides?

## Slide 60: Nanoparticle surfaces?
Oleic Acid Acetic Acid
1nm
SrO surface
PRL 111, 156101 (2013)
1nm
TiO2 DL
Profile imaging: L. D. Marks & D. J. Smith, Nature, 1983. 303 316
ANL ACAT

## Slide 61: Determined by solubility/chemisorption
Chart: 
| 0.5 | 1.5 | 1.5 | 1.5 | -0.5 | 1.2692307692307692 | 1.1000000000000001 | 1.3888888888888888
100 | 1.3727 | 1.7778 | 1.7028 | 1.4621 | 1.292 | 1.2389 | 1.3625 | 1.3313
 | 1.192 | 1.1389 | 1.3621
 | 1.392 | 1.3389 | 1.5621
SrO
Ö2
2x2
c4x2
TiO2
Ö13
Ö5
3x3
TiO2 per 1x1
eV/1x1 cell, revTPSSh
D. M. Kienzle, A. E. Becerra-Toledo, and L. D. Marks, PRL. 106, 176102 (2011)
Acetic Acid
Oleic Acid

## Slide 62: Glycerol Synthesis
4x1 Reconstruction on SrTiO3 {110} facets
SEM
HREM

## Slide 63: Wulff & Winterbottom
63
Increasing γint
Increasing γsub
Increasing γPt
J. A. Enterkin, K. R. Poeppelmeier, L. D. Marks, Nano Lett. 11, 993 (2011); G. Z. Wulff, Kristallogr. Mineral 34, 4490 (1901); W. L. Winterbottom, Acta Metallurgica 15, 303 (1967)
45° rotation around [100]
Projection down [010]
Projection down [110]
γ100
100
001
γ111
γ111
γ111
001
110
γInt – γSub = 0
γInt – γSub ≤ -γPt
-γPt < γInt – γSub < 0
γInt – γSub = γPt
0 < γInt – γSub < γPt

## Slide 64: Propane Oxidation
Pt/SrTiO3 epitaxy stabilizes metallic Pt
  For particle of radius R DG=DGOx+3DgInt/2R
  More reactive Pt/PtOx core/shell structure in oxidizing conditions
  Flux of reactants also different for different surfaces
J. A. Enterkin et al,, ACS Catalysis 1, 629 (2011)
Chart: Temperature (°C)
| 25 | 50 | 75 | 100 | 125 | 150 | 175 | 200 | 225 | 250 | 275 | 300 | 325 | 350 | 375 | 400 | 425 | 450 | 475 | 500 | 525 | 550
Nanocubes Cycle 1 | 0 | 0 | 0 | 0 | 0 | 0.59132 | 1.9706 | 6.2393 | 21.3693 | 58.6607 | 75.2656 | 85.3478 | 91.2173 | 95.6237 | 97.8908 | 99.2388 | 100.0211 | 100.1789 | 99.9559 | 99.9618 | 100.5067 | 100.2013
Nanocubes Cycle 2 | 0 | 0 | 0 | 0 | 0.12506 | 0.66742 | 2.5068 | 7.8454 | 37.0971 | 62.0384 | 75.394 | 84.5059 | 90.0892 | 93.6365 | 96.5822 | 98.4803 | 99.5066 | 100.0231 | 100.2119 | 100.4662 | 100.1684 | 100.5609
Nanocubes Cycle 3 | 0 | 0 | 0 | 0 | 0.23957 | 0.64074 | 2.2422 | 7.3214 | 28.1959 | 56.2254 | 69.1507 | 78.9498 | 85.1363 | 89.8721 | 93.2419 | 95.6559 | 97.3368 | 98.6955 | 99.6002 | 99.7891 | 100.4768 | 100.6423
Nanocubes Cycle 4 | 0 | 0 | 0 | 0 | 0 | 0.56038 | 2.0502 | 7.2643 | 29.3597 | 55.4226 | 69.1758 | 77.9196 | 84.306 | 88.4441 | 91.7451 | 94.3038 | 96.3328 | 97.7205 | 99.0418 | 98.808 | 99.2207 | 99.7945
Powder Cycle 1 | 0 | 0 | 0 | 0 | 0 | 0.31169 | 0.36732 | 0.94058 | 1.8945 | 4.2965 | 8.5154 | 15.3258 | 25.3904 | 36.5296 | 47.3075 | 56.1887
Powder Cycle 2 | 0 | 0 | 0 | 0 | 0 | 0 | 0.53751 | 0.9932 | 2.4026 | 5.0151 | 9.4394 | 16.3008 | 25.3412 | 35.5785 | 45.2132 | 54.9185
Powder Cycle 3 | 0 | 0 | 0 | 0 | 0 | 0.14959 | 0.45555 | 1.1941 | 2.361 | 5.0269 | 9.369 | 16.4134 | 25.8246 | 36.1987 | 46.3036 | 55.8707 | 64.0287 | 70.4759 | 75.8885 | 79.6901 | 82.853 | 85.2465
Powder Cycle 4 | 0 | 0 | 0 | 0 | 0 | 0 | 0.60244 | 1.0792 | 2.3401 | 4.4779 | 8.2964 | 13.4538 | 20.0931 | 27.293 | 34.2376 | 41.3249 | 47.3833 | 53.0104 | 58.7655 | 64.6375 | 70.6224 | 77.0633
Cycle 1 | 1
Cycle 2 | 1
Cycle 3 | 1
Cycle 4 | 1

## Slide 65: Reality Checkpoint
The results shown are just the tip of the iceberg
There are many more kinetic/thermodynamic reconstructions
Coupling nanoparticles with oxide surfaces & catalysis is complex

## Slide 66: LaAlO3 (110) 3x1
XPS
Kienzle, Koirala & Marks, Surface Science 633. 60, 2015
Convex Hull with Al & H2O

## Slide 67: SrTiO3 (110)
2D Alloy
Z. Wang, A. Loon, A. Subramanian, S. Gerhold, E. McDermott, J. A. Enterkin, M. Hieckel, B. C. Russell, R. J. Green, A. Moewes, J. Guo, P. Blaha, M. R. Castell, U. Diebold1, and L. D. Marks, in preparation

## Slide 68: Take home message
Oxide surfaces are complex, but manageable
  Remember Pauling’s rules
  Local order of polyhedral units, not random
  Structure determined by a subtle interplay of entropy, kinetics and thermodynamics

## Slide 69: ….at an oxide surface
This cartoon is almost certainly far from reality about the surface structure
Mg3(VO4)2 Mg3V2O6 + 2Obulk
O
Mg
Mg
V
O
O
O
O
O
Mg
Mg
V
O
O
surface
bulk
alkane + Olattice olefin + water
(Reactants) (Products)
O=O
O2-
2e-
The activity and selectivity are
closely related to the structures
of the catalyst used.
Mg3V2O8
Mg3V2O6
[011]
[100]
H2 / propane
Typical cartoons/visuals used in the literature

## Slide 70: ….at a nanoparticle surface
This cartoon is almost certainly far from reality about the surface structure
Mg3(VO4)2 Mg3V2O6 + 2Obulk
O
Mg
Mg
V
O
O
O
O
O
Mg
Mg
V
O
O
surface
bulk
alkane + Olattice olefin + water
(Reactants) (Products)
O=O
O2-
2e-
The activity and selectivity are
closely related to the structures
of the catalyst used.
Mg3V2O8
Mg3V2O6
[011]
[100]
H2 / propane
Typical cartoons/visuals used in the literature
Perling & Parak, Phil. Trans. R. Soc. A (2010) 368, 1333

## Slide 71: Reality Checkpoint: Nanoparticles are complex too…
Pt segregation to corners/edges in Pt/Pd; L. Peng et al, PCCP DOI: 10.1039/C5CP01492A
Interfaces change during catalysis
Lin et al, Nano Lett., 2015, 15 (8), 5375
J. A. Enterkin et al, Nano Lett. 11, 993 (2011)
Broken symmetry
Lu Jiang
unpublished
Nanoparticles have round corners, Alpay et al, JPC, 2015;119(36):21018

## Slide 72
Questions ?
Research is to see what everybody else has seen, and to think what nobody else has thought Albert Szent-Györgi