## Slide 1: Nanoparticles: from Wulff to Winterbottom and Beyond
Subtitle
Something old, something new, a lot borrowed, a lot purple
http://www.numis.northwestern.edu/Presentations

## Slide 2: Acknowledgements 1
Phase 1: 1978-1994
  E. Yoffe, A. Howie, D. J. Smith, J. M. Cowley, J. Dundurs
  P. M. Ajayan, D. Iyer

## Slide 3: Acknowledgements 2
Phase 2: 2008-
K. R. Poeppelmeier R. Van Duyne
J. Enterkin E. Ringe B. Peng D. Alpay S. Patala
Materials Research Science & Engineering Center
Northwestern University
Notes: 3

## Slide 4: Small can be beautiful
Pro’s
  Nanoplasmonics
  Nanoparticles for catalysis
  Sensing
  Drug delivery
  …
Image Source:
John Stringer
Electric Power Research Institute
Notes: 4

## Slide 5: Nanosized Gold
www.notredamedeparis.fr
L. Liz-Marzan, Mater. Today 7, 21 (2004)
Notes: 5

## Slide 6: Small can be ugly
Con’s
  Toxic
  Wear Debris
Hip Implant
Liao et al., Science 334, 1687 (2011)
Notes: 6
6

## Slide 7: Wear-Mediated Osteolysis
osteoblast
osteoclast/ polymorphonuclear giant cell
http://academic.brooklyn.cuny.edu/biology/bio4fv/page/aviruses/cellular-immune.html
Archibeck, MJ; Jacobs, JJ; Roebuck, KA; Glant, TT. Journal of Bone & Joint Surg, 2000
wear particles
osteolysis
opsonization
phagocytosis
disrupted balance between osteoclasts/PMNs and osteoblasts:
osteoclasts ↑, osteoblasts ↓

## Slide 8: Nanoparticle Crystallography from 100 nm down
Some basics that everyone should know
  Wulff, Winterbottom and friends
Some basics that most do not know or get wrong
  The artifact of some particle size effects
  There are two Wulff constructions
Some new basics
  Segregation in nanoparticles and with strain
One application – catalysts by design

## Slide 9: Basics: Continuum, simple
The total energy of an ordered, crystalline nanoparticle can be written as
Bulk Surface Edge Corner
Thermodynamic shape for reasonable sizes minimizes E at a fixed volume
Find the shape that optimizes the surface energy

## Slide 10: Wulff Construction
Minimize surface energy for fixed volume
Max Von Laue
G. Z. Wulff, Kristallogr. Mineral 34, 4490 (1901); M. Z. Von Laue, Kristallogr. 105, 124 (1943); A. Z. Dinghas, A. Z. Kristallogr. 105, 304 (1944)

## Slide 11: Example: Gold Octahedra
C. Li, K. L. Shuford, M. Chen, E. J. Lee, S. O. Cho, ACS Nano. 2, 1760 (2008)
Notes: 11

## Slide 12: Chemisorption Dependent
Cu Bi-saturated Cu
Curtesy Paul Wynblatt

## Slide 13: Winterbottom Construction
gInt
Include the effect of a nanoparticle sitting on a substrate
N.B., Kaischew may be a better source, unclear

## Slide 14: Wulff & Winterbottom
14
Increasing γint
Increasing γsub
Increasing γPt
J. A. Enterkin, K. R. Poeppelmeier, L. D. Marks, Nano Lett. 11, 993 (2011); G. Z. Wulff, Kristallogr. Mineral 34, 4490 (1901); W. L. Winterbottom, Acta Metallurgica 15, 303 (1967)
45° rotation around [100]
Projection down [010]
Projection down [110]
γ100
100
001
γ111
γ111
γ111
001
110
γInt – γSub = 0
γInt – γSub ≤ -γPt
-γPt < γInt – γSub < 0
γInt – γSub = γPt
0 < γInt – γSub < γPt
51° rotation around [011]

## Slide 15: Caveat: assumes flat substrate
Connects to strong metal support interactions (SMSI)
Ajayan, P.M. and L.D. Marks, Nature, 1989. 338(6211), 139

## Slide 16: Basics: Continuum, not so simple
The total energy of an ordered, crystalline nanoparticle can be written as
The ni are positive integers represent the number of atoms along particular directions. Which term is “bulk”, which term is “surface” ?

## Slide 17: Counting Effects
Number of Atoms
= n(n+1)/2
Not n2 dependence
n

## Slide 18: Wulff shape apparently size dependent
Marks, L.D., Surface Science, 1985. 150(2), 358; Bonevich, J.E., Proc 47th Ann EMSA, 1989, 258.

## Slide 19: What is the size?
Crystallographic Size
Chemisorption Size
C=O
Thermodynamic Size
V = constant*N

## Slide 20: Care needed
Based on, but not the same as Hamilton, Phys. Rev. B, 2006. 73: 125447, see also Cleveland and Landman JCP, 1991. 94(11), 7376
Simplest approach, define distances such that V(h) = Nvatom
Introduces a non-linear relationship between h & N
Adds some minor corrections
Equimolar Gibbs surface using Wigner-Seitz cells

## Slide 21: Simplification
Bulk Surface Edge Corner
Rewrite as
WD Strain Energy Density
Dimensionless shape term
Surface Stress Contribution

## Slide 22: Surface Energy & Stress I
Important: never use the term “surface tension” for a solid. Never. Really never.
Surface (Free) Energy γ
  Define as energy to create new fully relaxed surface
  Different from cleavage energy
  Caveat: definition “per area” or “per atom” are not the same – thermodynamic & DFT definitions can differ

## Slide 23: Surface Energy & Stress II
Surface Stress
  Derivative with strain
  Tensor
  Care needed with how strains are defined (endless confusion in literature)
  Vanishes for a normal liquid
  This is the term that leads to “pressure” (lattice changes) in nanoparticles

## Slide 24: Weighted Mean Curvature
With Es total surface energy:
=
=
Equilibrium
;
;
The same as Wulff construction (Lagrangian)
For an alloy, , each component j
e.g. Taylor, J.E., Acta Met., 1992. 40(7): p. 1475-1485.

## Slide 25: Geometric interpretation
hi
ri
{ar1+b} /{cri2+dri+e}
 /ri
Nominal equivalent of Gibbs-Thompson term, but for a faceted surface. Suggests that corners are rarely sharp, observed experimentally

## Slide 26: Continuing, beyond single crystals
Reduce surface energy, at the cost of strain energy
Decahedral MTP Icosahedral MTP

## Slide 27: But…Dh is not so simple
L. D. Marks,. Philos. Mag. A. 49, 81 (1984).

## Slide 28: Modified Wulff Construction
L. D. Marks,. Philos. Mag. A. 49, 81 (1984).

## Slide 29: Modified Wulff Construction for Twinned Particles
L. D. Marks, J. Cryst. Growth 1983, 61, 556-566
Lamellar Twinned Particles
2 or more segments
1 boundaries/segment (caps)
2 boundaries/segment (middle)
Decahedral
Multiply Twinned Particle
5 segments
2 boundaries/segment
Icosahedral
Multiply Twinned Particle
20 segments
3 boundaries/segment
Notes: 29

## Slide 30: Shapes for Dh reported in 19th century
From H. Hofmeister, Z Krist 224 (2009) 528

## Slide 31: Different Cases
E. Ringe, R.P. Van Duyne, L. D. Marks, Journal of Physical Chemistry C, 2013. 117, 15859

## Slide 32: Different Shapes for Ic as well
Images courtesy of M. Yacaman
{111} only
{110} only
{111} + {110}
N.B., no {100} in an Ic, see L. D. Marks, Philos. Mag. A. 49, 81 (1984)

## Slide 33: Surfaces depend upon environment
“5x1” (001) reconstruction on Au Dh, Image courtesy of Gilberto Casillas-Garcia, UTSA

## Slide 34: MTP Energetics
Three Terms
  Strain, fcc units do not fit together without it
  Difference in total surface free energy
  Difference in total surface stress terms
  N.B., twin boundary energy negligable

## Slide 35: Strain: Volterra Disclination
Von Mises stress distribution (a)
R. de Wit, Journal of Physics C, 1972, 5, 529
A. Howie and L. D. Marks, Phil Mag 1984. 49(1), 95-109.
Patala, S., L.D. Marks, and M.O. de la Cruz, Journal of Physical Chemistry C, 2013. 117(3), 1485
S. Ogawa & S. Ino, J. Vac. Sci. Tech. 6, 527 (1969).

## Slide 36: MTPs have less of the Wulff shape
Twin boundaries restrict which surfaces are exposed
L. D. Marks,. Philos. Mag. A. 49, 81 (1984).
Segment for Dh

## Slide 37: Energy Balance
Three competing terms
  Gain in surface energy (MTPs more {111})
  Cost to strain the particle
  Energy change due to expansion at surface, surface stress term (heavily environment dependent)
Chart: 
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20
Sc | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5
Dh | 3.15 | 3.3 | 3.45 | 3.6 | 3.75 | 3.9 | 4.05 | 4.2 | 4.35 | 4.5 | 4.65 | 4.8 | 4.95 | 5.1 | 5.25 | 5.4 | 5.55 | 5.7 | 5.85 | 6
Ic | 2.3 | 2.6 | 2.9 | 3.2 | 3.5 | 3.8 | 4.1 | 4.4 | 4.7 | 5 | 5.3 | 5.6 | 5.9 | 6.2 | 6.5 | 6.8 | 7.1 | 7.4 | 7.7 | 8
A. Howie and L. D. Marks, Phil Mag 1984. 49(1), 95-109.
Ic Dh Sc

## Slide 38: Energetics
Icosahedra
Quasi-spherical shape.
Close-packed surface but
large internal strain.
Favourable at small sizes
Decahedra
Intermediate behaviour.
Favourable at
Intermediate sizes
Polyhedra
Non-spherical shape
No internal strain.
Favourable at large sizes
Courtesy Riccardo Ferrando

## Slide 39: Structural Fluctuations (Iijima)
P. M. Ajayan, L. D. Marks,. 24-6, 229 (1990)

## Slide 40: A simple physical concept
Courtesy of Stephen Berry
The potential surface, very schematically: solid in the deep, narrow well, liquid in the high rolling plain:

## Slide 41: Quasimelting
J. Dundurs, L. D. Marks, P. M. Ajayan,. Philos. Mag. A. 57, 605 (1988)

## Slide 42: Morphological Transitions (Angus Kirkland)
Room temp
300°C
400°C
FCC
Decahedral
RT
400°C
RT
Icosahedral
Decahedral
In-situ Heating
RT
400°C
RT
Decahedral
Decahedral
5.5nm size
7.2nm size
10.4nm size
Ultramicroscopy, 110 (2010) 506
ACS Nano, 3 (2009) 1431
Solid – Solid Transition below Tm
As Synthesised Particles not in Thermodynamic Ground State

## Slide 43: Phase Diagram (1990 vintage)
P. M. Ajayan, L. D. Marks. Phase Transit. 24-6, 229 (1990)

## Slide 44: The Two Wulff Constructions
Just to make life more fun
  Is every Wulff shape thermodynamic?
  No, and probably the original paper was not a thermodynamic case!

## Slide 45: Thermodynamic Wulff Construction
γ = surface free energy
n = crystallographic face (hkl)
h(n) = surface normal
Λ(c) = Wulff constant (accounts for volume)
γ100
γ111
001
110
100
001
γ111
G. Z. Wulff, Kristallogr. Mineral. 34, 449 (1901)
Notes: 45

## Slide 46: Kinetic Wulff Construction
v= growth velocity
n = crystallographic face (hkl)
h(n) = surface normal
Λ(c) = Wulff constant (accounts for volume)
γ100
γ111
001
110
100
001
γ111
Frank, F. C. In Growth and Perfection of Crystals; Wiley (1958)
Notes: 46

## Slide 47: Kinetic v Thermodynamic Wulff
i depends upon
Chemisorption
Surface Composition
Bulk Composition
Surface Segregation
vi depends upon
Rate limiting step (diffusion/nucleation)
Transition state (e.g. desorption of surfactants)
, i.e. local chemical potential

## Slide 48: Origin of twin enhancement term
Atoms added at a twin have a higher co-ordination number than on a flat surface
Additional energy makes nucleation easier
Gamalski et al, Nano Lett 2014, 14, 1288
Atom bonds to those on both sides

## Slide 49
Kinetic Wulff Construction for Twinned Particles
Kinetic Wulff: Growth Velocity
Twinned Wulff: Assemble Segments
+ Growth enhancement
Frank, F. C. In Growth and Perfection of Crystals; Doremus, Wiley (1958)
L. D. Marks, J. Cryst. Growth 61, 556 (1983) ;E. Ringe, R.P. Van Duyne, L. D. Marks, JPC C, 2013. 117, 15859
Re-entrant surface growth enhancement
Disclination/twin boundary growth enhancement
5X
=

## Slide 50
Re-entrant growth
Disclination + re-entrant
100 nm
B. Petrobon, M. McEachran, V. Kitaev, ACS Nano 2009, 3, 21-26
Modified Kinetic Wulff Construction:
Shape of Dh Structures
111
100
γ111/ γ100 = 3/2
Re-entrant + Stable 111
Notes: 50

## Slide 51
Modified Kinetic Wulff Construction:
Shape of {111} – Dominated Monotwin Structures
Twin growth enhancement
Twin + re-entrant growth enhancement
Re-entrant surface growth enhancement
Notes: 51

## Slide 52: Alloy Wulff Construction
Alloy Wulff has an extra degree of freedom: surface composition
Use available/measurable parameters (surface/bulk energies) to produce a predictive model
Result of energy minimization: size-dependant balance between
  Surface energy
  Starvation energy
γ100
γ111
001
110
100
001
γ111
E. Ringe, R.P. Van Duyne, L. D. Marks, Nano Lett. 11, 3399 (2011)
Notes: 52

## Slide 53
Alloy Wulff Construction:
Minimization of Energy via Lagrangian Multipliers
γ = surface free energy
n = crystallographic face
CSi = surface concentration of element i
CVi = bulk concentration
G = bulk free energy
Λ = Wulff constant (accounts for volume)
hn = surface normal
Conventional Wulff
Alloy Wulff
γ = surface free energy
n = crystallographic face
hn = surface normal
Λc = Wulff constant (accounts for volume)
Size Independent
Size Dependent: Starvation
h(100)
h(110)

## Slide 54: Comparison of Methods
Conventional Wulff
X Segregation
X Starvation
Infinite Reservoir
Segregation
X Starvation
Alloy Wulff
Segregation
Starvation
Surface
Bulk

## Slide 55
Alloy Wulff Construction for Weak Alloy AgAu
Surface
Bulk
Surface
Bulk
γAu > γAg
Monolayer formation De-alloying
Notes: 55

## Slide 56
3 Regimes in CuAu Alloy Wulff Construction
1 2 3
1 2 3
1: De-alloying 2: Bulk/surface equilibrium 3: Monolayer formation
γAu < γCu
Notes: 56

## Slide 57: Can we exploit these ideas
57
NO on Pt Masel, 1983
Winterbottom construction, different exposed facets
Substrate
J. A. Enterkin, K. R. Poeppelmeier, L. D. Marks, Nano Lett. 11, 993 (2011);

## Slide 58: Propane Oxidation
Pt/SrTiO3 epitaxy stabilizes metallic Pt
  For particle of radius R DG=DGOx+3DgInt/2R
  More reactive Pt/PtOx core/shell structure in oxidizing conditions
  Flux of reactants also different for different surfaces
J. A. Enterkin et al,, ACS Catalysis 1, 629 (2011)
Chart: Temperature (°C)
| 25 | 50 | 75 | 100 | 125 | 150 | 175 | 200 | 225 | 250 | 275 | 300 | 325 | 350 | 375 | 400 | 425 | 450 | 475 | 500 | 525 | 550
Nanocubes Cycle 1 | 0 | 0 | 0 | 0 | 0 | 0.59132 | 1.9706 | 6.2393 | 21.3693 | 58.6607 | 75.2656 | 85.3478 | 91.2173 | 95.6237 | 97.8908 | 99.2388 | 100.0211 | 100.1789 | 99.9559 | 99.9618 | 100.5067 | 100.2013
Nanocubes Cycle 2 | 0 | 0 | 0 | 0 | 0.12506 | 0.66742 | 2.5068 | 7.8454 | 37.0971 | 62.0384 | 75.394 | 84.5059 | 90.0892 | 93.6365 | 96.5822 | 98.4803 | 99.5066 | 100.0231 | 100.2119 | 100.4662 | 100.1684 | 100.5609
Nanocubes Cycle 3 | 0 | 0 | 0 | 0 | 0.23957 | 0.64074 | 2.2422 | 7.3214 | 28.1959 | 56.2254 | 69.1507 | 78.9498 | 85.1363 | 89.8721 | 93.2419 | 95.6559 | 97.3368 | 98.6955 | 99.6002 | 99.7891 | 100.4768 | 100.6423
Nanocubes Cycle 4 | 0 | 0 | 0 | 0 | 0 | 0.56038 | 2.0502 | 7.2643 | 29.3597 | 55.4226 | 69.1758 | 77.9196 | 84.306 | 88.4441 | 91.7451 | 94.3038 | 96.3328 | 97.7205 | 99.0418 | 98.808 | 99.2207 | 99.7945
Powder Cycle 1 | 0 | 0 | 0 | 0 | 0 | 0.31169 | 0.36732 | 0.94058 | 1.8945 | 4.2965 | 8.5154 | 15.3258 | 25.3904 | 36.5296 | 47.3075 | 56.1887
Powder Cycle 2 | 0 | 0 | 0 | 0 | 0 | 0 | 0.53751 | 0.9932 | 2.4026 | 5.0151 | 9.4394 | 16.3008 | 25.3412 | 35.5785 | 45.2132 | 54.9185
Powder Cycle 3 | 0 | 0 | 0 | 0 | 0 | 0.14959 | 0.45555 | 1.1941 | 2.361 | 5.0269 | 9.369 | 16.4134 | 25.8246 | 36.1987 | 46.3036 | 55.8707 | 64.0287 | 70.4759 | 75.8885 | 79.6901 | 82.853 | 85.2465
Powder Cycle 4 | 0 | 0 | 0 | 0 | 0 | 0 | 0.60244 | 1.0792 | 2.3401 | 4.4779 | 8.2964 | 13.4538 | 20.0931 | 27.293 | 34.2376 | 41.3249 | 47.3833 | 53.0104 | 58.7655 | 64.6375 | 70.6224 | 77.0633
Cycle 1 | 1
Cycle 2 | 1
Cycle 3 | 1
Cycle 4 | 1

## Slide 59: Nanoparticle surfaces?
Oleic Acid Acetic Acid
1nm
SrO surface
PRL 111, 156101 (2013)
1nm
TiO2 DL

## Slide 60: Summary
While we know at lot from old work (even back to Gibbs)
Care is needed (many errors in literature)
  Being precise with size matters
Nanoalloys has some new possibilities
Still some things that are not fully understood

## Slide 61: But
All details how surface structure & segregation couples to nanoparticle structure not clear yet
Everthing becomes richer (but manageable) when chemisorption is included
Often there are no precise measurements of structure to match to models
And how this couples to rates/selectivity…

## Slide 62: Questions ?
Research is to see what everybody else has seen, and to think what nobody else has thought Albert Szent-Györgi