## Slide 2: Oxide Surfaces Opening the Pandora’s Box for SrTiO3
L. D. Marks
Surfaces
DFT
Structure
10 nm
NanoCatalysts
Catalysis

## Slide 3: Acknowledgements
TEM: N. Erdman (JEOL), A. Subramanian (Intel), A. Chiaramonti (NIST), A. Becerra (Dow), J. Enterkin (Philips 66), D. Keinzle (Premier International), Y. Lin
DFT: A. Becerra, J. Enterkin, D. Keinzle, Y. Lin & LDM
STM Simulations: A. Becerra
Synthesis: L. Hu, Y. Lin, C. Wang
Catalysis: L. Hu, Y. Lin, C. Wang
Collaborators:
K. Poeppelmeier (NU), P.C. Stair (NU), P. Blaha (Vienna), M. Castell (Oxford), O. Warschkow (U. Sydney), U Diebold (Vienna)

## Slide 4: Motivation
Oxide surfaces are everywhere:
  Everything in this room
  Active catalysts
  Catalytic supports
  Photocatalysts
  Multiferroic Oxides
  Solid Oxide Fuel Cells
  Corrosion products
  Buildings (cement)
Baha’i Temple, Wilmette

## Slide 5: Looking to the future
Need to better understand catalysts and oxide surfaces:
Convert light petroleum and coal to useful products
Convert biomass to gasoline
Convert carbon dioxide into liquid fuels
Low-power oxide electronics
Image Source:
John Stringer
Electric Power Research Institute

## Slide 6: Catalytic Schematics
This cartoon is almost certainly far from reality about the surface structure
Mg3(VO4)2 Mg3V2O6 + 2Obulk
O
Mg
Mg
V
O
O
O
O
O
Mg
Mg
V
O
O
surface
bulk
alkane + Olattice olefin + water
(Reactants) (Products)
O=O
O2-
2e-
The activity and selectivity are
closely related to the structures
of the catalyst used.
Mg3V2O8
Mg3V2O6
[011]
[100]
H2 / propane
Overall Objective: To characterize and identify the active site(s) for oxidative dehydrogenation; reductive addition and oxidative elimination.

## Slide 7: Broad Vision
Time
Discovery-based
Time
Oxide Nanocatalysts By Design
Adapted From: Paget Donnelly, Nanomaterials By Design, Chemical Industry R&D Roadmap, www.chemicalvision2020.org/downloads/nanochemroadmap_presentation_1-5-04.ppt

## Slide 8
Ti
(110)
Single Crystal
Growth
TEM & Electron Diffraction
Direct Methods & DFT
Ti
O
Sr
10 nm
Nanoparticle
Synthesis
Surface
Structure
Catalytic Oxides
Catalytic
Activity
Thermodynamics
Bridge the Materials Gap

## Slide 9: Basics
100-300 keV
Both give kinematical data for surfaces

## Slide 10: Core experimental technique
Incident 100-300 kV electrons
Collect images or diffraction information
+SXRD, STM if available

## Slide 11: UHV-TEM & Vacuum Chamber

## Slide 12: Configuration & Operation
UHV-H9000
5-10x10-11t @ 300kV
Metal Evaporator
Load-lock
BN 5x10-11t
Gas Cell
600C, 1 atmosphere
Analytical
Chamber
5x10-11t
MIBE 1x10-9t
CN growth
Transfer
Chamber 1x10-11 t
X
Load Sample
X
Clean
Check Sample
X
X
Deposit BN
X
HREM

## Slide 13: Sample preparation (an art)
Cut 3mm disc or mount sample
Dimple thin to 10 mm
Thin to < 0.1 mm
  Ion beam (damage)
  Chemical (?)
Anneal damage (carefully!)
Last step similar to making new oxides
  Try a time/temperature: if it works, celebrate
  If it does not, try again…..
  All you need are enough slaves grads/undergrads
Dimple Wheel
Sample

## Slide 14: SrTiO3 (111): Pre-annealing
Sample is under stress, disordered, and non-stoichiometric
(110)
100 nm
diffuse ring
~100 Å
[111]
A. N. Chiaramonti et al., Surf. Sci. 602, 3018 (2008).

## Slide 15: Annealing
In-situ
Ex-situ

## Slide 16: SrTiO3 (111): Annealed
Surfaces are:
  ordered, flat
  covered in large often triangular terraces and step bunches
Reconstructed
Air stable (months)
Reproducible
100 nm
A. N. Chiaramonti et al., Surf. Sci. 602, 3018 (2008).

## Slide 17: Measured Intensities
Weak dynamical effects
Chart: Low Loss Peels Spectrum
Chart: Average
 | 150 | 14150
 | -150 | 13850
Errors (repeat measurements)
EELS, thickness

## Slide 18: How to solve a structure?
Guess, then refine
  Will always give something, but if the guess is wrong GIGO
Use Patterson function
  Difficult for complicated structures
Get an image
  STM is hard to interpret
  HREM is difficult for surfaces (and not always possible)
Use DFT
  If the original guess is wrong, GIGO
  Functionals can be (very) inaccurate for oxides
Try something else?

## Slide 19: Diffraction Phase Problem
F(h) = |F(h)|exp[2i(h)]
FFT
Surface r(r)
Unmeasured
Measured diffraction intensities
|F(h)| = [I(h)]1/2
An equal opportunity problem – true for x-ray and electron diffraction

## Slide 20: Phase: Apples & Oranges
FT Aa exp(-i a)
Ao exp(-i a) IFT
FT Ao exp(-i o)
+
{
Oranle ?
Appge ?
Phase of Apple + Amplitude of Orange = ?

## Slide 21: Phase of Apple = Apple
FT-1 {Ao exp(-i a) }
Apple
Phase is more important than amplitude

## Slide 22: Direct Methods vs. Indirect Methods
Indirect Methods:
“Trial and Error”
Direct Methods:
Using available information
to find solutions

## Slide 23: Second Core: Direct Methods
Feasible Solution
Fourier Transform
Inverse
Fourier Transform
Impose Fourier space
constraints (S2)
Impose real space
constraints (S1)
Observed Intensities
(assigned phases)
(Global Search)
Recovery
Criterion
YES
NO
Atoms
Intensities
L. D. Marks, W. Sinkler, and E. Landree, Acta Cryst A55, 601 (1999) L. D. Marks, Phys. Rev. B 60, 2771 (1999)
L. D. Marks et al., Surf. Rev. Lett. 5, 1087 (1998).

## Slide 24: Ag on Ge (111) 4x4
[110]
[112]
Collazo-Davila et al, Surface Science 418, 395 (1998)
X-ray data

## Slide 25: InSb c8x2
C. Kumpf, et al, Physical Review Letters 86, 3586 (2001)

## Slide 26: Aim
Infinite Number of Possible
Arrangements of
Atoms
Finite
R, 2, structure, DFT and chemistry
Direct Methods

## Slide 27: Third Key Tool: DFT
Has become (alas?) almost a black-box method
GIGO – DFT only refines, it is not a search method (which Direct Methods are)
DFT energies have serious errors for oxides
  Need to calibrate errors, and understand them (~0.1eV/1x1 cell)
  Need to use higher-order functionals (not just PW91/PBE or even PBEsol) such as meta-GGA and/or hybrids (exchange corrections)

## Slide 28: Four examples
Connect TED, DFT, STM (and chemistry); the SrTiO3 (110) surface
What lies beyond order: glass-like tilings on SrTiO3, the Ö13xÖ13 (001) reconstruction
Surface Structure of Nanocuboid SrTiO3
Some additional complications: SrTiO3 (111), water and beyond

## Slide 29: Four examples
Connect TED, DFT, STM (and chemistry); the SrTiO3 (110) surface
What lies beyond order: glass-like tilings on SrTiO3, the Ö13xÖ13 (001) reconstruction
Surface Structure of Nanocuboid SrTiO3
Some additional complications: SrTiO3 (111), water and beyond

## Slide 30: SrTiO3 (110): 900C in O2
40 nm
001
1x1
30
N. Erdman, PhD Thesis, 2002
Dark Field

## Slide 31: 1000 °C in flowing O2
DP’s from Arun Subramanian
_
(110)
(001)
1x1
3
1

## Slide 32: Direct Methods Solution

## Slide 33: Atomic Positions Refined
33

## Slide 34: SrTiO3 (110) 3x1
TiO2 overall surface stoichiometry
  Ti5O7 atop O2 termination
  Ti5O13 atop SrTiO termination
Surface composed of corner sharing TiO4 tetrahedra
  Arranged in rings of 6 or 8 tetrahedra
  4 corner share with bulk octahedra
  1 edge shares with bulk octahedron
Enterkin et. al., Nature Materials, 2010
Blue polyhedra are surface polyhedra, gold are bulk octahedra, orange spheres Sr, blue spheres Ti, red spheres O

## Slide 35: SrTiO3 (110) nx1
3x1
4x1
∞x1
2x1
3x1
4x1
5x1
6x1
Expansion to other nx1 by changing the number of TiO4 surface tetrahedra per ring
Notes: Talk about composition of each
First observation of homologous series on a surface

## Slide 36: Intergrowths
STM with simulations (DFT)
Enterkin et. al., Nature Materials, 2010
4x1
3x1
3x1
6x1
5x1
6x1
4x1
4x1
5x1

## Slide 37: SrTiO3 (110) 3x1
Bond valence sums
  Ti1 = 4.04
  Ti2 = 4.08
  Ti3 = 4.04
  O1 = 2.03-
  O2 = 2.02-
  O3 = 2.04-
  O4 = 2.19-
Enterkin et. al., Nature Materials, 2010
Blue polyhedra are surface polyhedra, gold are bulk octahedra, orange spheres Sr, blue spheres Ti, red spheres O
Ti1
Ti2
Ti3
O1
O2
O3
O4
Explanation: Pauling’s Rules (BVS)
The principles determining the structure of complex ionic crystals. J. Am. Chem. Soc. 51 (4): 1010 1929.

## Slide 38: STO (110) Bond Valence Sums
Bond Valence |  | Sr | Half-O2 | ¥x1 | 6x1 | 5x1 | 4x1 | 3x1 | 2x1
Surf | Ti(Sr) | 1.88 | 3.83 | 3.41 | 3.87 | 3.93 | 3.99 | 4.06 | 4.02
Surf | O | 1.49- | 1.94- | 1.21- | 1.88- | 1.95- | 1.99- | 2.05- | 2.07-
Sub-surf | O | 2.61- | 1.88- | 2.07- | 2.02- | 2.04- | 2.05- | 2.05- | 1.94-
Chart: 
| -1 | 0 | 1.3333333333333333
 | 0.88982 | 0 | -0.23755
 | 0.88982 | -0.23755 | -0.29244 | -0.33782 | -0.2011 | 0.44465
Surface Energy
(eV per 1x1 unit)
X: TiO2 at Surface
SrO monolayer
at Surface
TPSSh

## Slide 39: Four examples
Connect TED, DFT, STM (and chemistry); the SrTiO3 (110) surface
What lies beyond order: glass-like tilings on SrTiO3, the Ö13xÖ13 (001) reconstruction
Surface Structure of Nanocuboid SrTiO3
Some additional complications: SrTiO3 (111), water and beyond

## Slide 40: STiO3 (001) Energies
Chart: 
| 0.5 | 1.5 | 1.5 | 1.5 | -0.5
100 | 1.3727 | 1.79 | 1.6977 | 1.4621 | 1.292
 | 1.192 | 1.2727 | 1.3621
 | 1.392 | 1.4727 | 1.5621
SrO
Ö2
2x2
c4x2
TiO2
TiO2 per 1x1
eV/1x1 cell, revTPSSh
(001)
2x1 2x2 Ö2xÖ2 c4x2 c6x2 √5x√5 √13x√13
For errors, see L. D. Marks et al., Surf. Sci. 603, 2179 (2009) For revTSPP J.P. Perdew, PRL 103, 026403 (2009)

## Slide 41: Common features: 1x1 Base
Building Blocks:
5-fold Ti 6-fold Ti
Top View Side View
Sr (not critical)

## Slide 42: 2x2 Structure
O. Warschkow et al., Surf. Sci. 573, 446 (2004).
Top View Side View

## Slide 43: Ö2xÖ2 R45
O. Warschkow et al., Surf. Sci. 573, 446 (2004).
Top View Side View

## Slide 44: c(4x2)
N. Erdman et al., J. Am. Chem. Soc. 125, 10050 (2003).
Top View Side View

## Slide 45: STiO3 (001) Energies
Chart: 
| 0.5 | 1.5 | 1.5 | 1.5 | -0.5
100 | 1.3727 | 1.79 | 1.6977 | 1.4621 | 1.292
 | 1.192 | 1.2727 | 1.3621
 | 1.392 | 1.4727 | 1.5621
SrO
Ö2
2x2
c4x2
TiO2
TiO2 per 1x1
eV/1x1 cell, revTPSSh
(001)
2x1 2x2 Ö2xÖ2 c4x2 c6x2 √5x√5 √13x√13
Intermediate compositions?
For errors, see L. D. Marks et al., Surf. Sci. 603, 2179 (2009) For revTSPP J.P. Perdew, PRL 103, 026403 (2009)

## Slide 46: Ö13xÖ13 R33.7 SrTiO3 (100)
Make a “normal” sample
Buffer-etched then annealed
Changes surface TiO2 excess
D. M. Kienzle, A. E. Becerra-Toledo, and L. D. Marks,
Phys. Rev. Lett. 106, 176102 (2011)

## Slide 47: (001) Ö13xÖ13 Initial Map

## Slide 48: (001) Ö13xÖ13 Refined

## Slide 49: Other tilings
Ö13xÖ13
3x3
Ö5xÖ5
D. M. Kienzle, A. E. Becerra-Toledo, and L. D. Marks, PRL. 106, 176102 (2011)

## Slide 50: c4x2 (left) and Ö5xÖ5 (right)
STM: Castell Surface Science 505 (2002) 1–13

## Slide 51: STiO3 (001) Energies
Chart: 
| 0.5 | 1.5 | 1.5 | 1.5 | -0.5
100 | 1.3727 | 1.7778 | 1.7028 | 1.4621 | 1.292
 | 1.192 | 1.2727 | 1.3621
 | 1.392 | 1.4727 | 1.5621
SrO
Ö2
2x2
c4x2
TiO2
TiO2 per 1x1
eV/1x1 cell, revTPSSh

## Slide 52: Stable according to DFT
Chart: 
| 0.5 | 1.5 | 1.5 | 1.5 | -0.5 | 1.2692307692307692 | 1.1000000000000001 | 1.3888888888888888
100 | 1.3727 | 1.7778 | 1.7028 | 1.4621 | 1.292 | 1.2389 | 1.3625 | 1.3313
 | 1.192 | 1.1389 | 1.3621
 | 1.392 | 1.3389 | 1.5621
SrO
Ö2
2x2
c4x2
TiO2
Ö13
Ö5
3x3
TiO2 per 1x1
eV/1x1 cell, revTPSSh
Glasses
D. M. Kienzle, A. E. Becerra-Toledo, and L. D. Marks, PRL. 106, 176102 (2011)

## Slide 53: Four examples
Connect TED, DFT, STM (and chemistry); the SrTiO3 (110) surface
What lies beyond order: glass-like tilings on SrTiO3, the Ö13xÖ13 (001) reconstruction
Surface Structure of Nanocuboid SrTiO3
Some additional complications: SrTiO3 (111), water and beyond

## Slide 54: Nanoparticle surfaces?
PRL 111, 156101 (2013)
Oleic Acid Acetic Acid

## Slide 55: Profile Imaging
Area 2
Area 1
ACAT at ANL

## Slide 56: Numbers, numbers, numbers
Images are for artists
Signals are for scientists
Chart: oscillation vs thickness
| 33.6 | 39.200000000000003 | 44.8 | 50 | 56 | 61
simulation | 0.027282 | 0.029101 | 0.034612 | 0.041294 | 0.052341 | 0.07003
Gaussian Fit

## Slide 57: Surfaces, surfaces, surfaces
Vibration
40 picometers
(Image Spread?)
MacTempas

## Slide 58: Nanoparticle surfaces?
Oleic Acid Acetic Acid
1nm
SrO surface
PRL 111, 156101 (2013)
1nm
TiO2 DL

## Slide 59: Nanoparticle surfaces?
Chart: Interlayer numbers (i)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9
Perfect | 1.9764 | 1.9259 | 1.9799 | 1.9246 | 1.9863 | 1.9182 | 2.004 | 1.9007 | 2.0056 | 0 | 1.9741 | 1.9237 | 1.9775 | 1.9224 | 1.984 | 1.9159 | 2.0017 | 1.8985 | 2.0033
To Bulk
PRL 111, 156101 (2013)
Not for the faint hearted....
1nm
SrO surface

## Slide 60: Nanoparticle surfaces?
Chart: Interlayer numbers (i)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9
EXP | 1.7529 | 2.0748 | 1.9533 | 1.924 | 2.0071 | 1.9094 | 1.9923 | 1.9165 | 1.9918
Perfect | 1.9764 | 1.9259 | 1.9799 | 1.9246 | 1.9863 | 1.9182 | 2.004 | 1.9007 | 2.0056 | 0 | 1.9741 | 1.9237 | 1.9775 | 1.9224 | 1.984 | 1.9159 | 2.0017 | 1.8985 | 2.0033
PRL 111, 156101 (2013)
Not for the faint hearted....
To Bulk
1nm
SrO surface

## Slide 61: Nanoparticle surfaces?
Precision good enough – functional matters!
Chart: Interlayer numbers (i)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9
PBEsol0 | 1.7755 | 2.0132 | 1.939 | 1.9438 | 1.9794 | 1.9282 | 1.9905 | 1.9182 | 1.9913
EXP | 1.7529 | 2.0748 | 1.9533 | 1.924 | 2.0071 | 1.9094 | 1.9923 | 1.9165 | 1.9918
PBE | 1.742 | 2.042 | 1.9141 | 1.9504 | 1.9678 | 1.9283 | 1.9863 | 1.9181 | 1.9906
To Bulk
PRL 111, 156101 (2013)
1nm
SrO surface

## Slide 62: Nanoparticle surfaces?
Precision good enough – functional matters!
To Bulk
PRL 111, 156101 (2013)
Chart: absolute cumulative errors
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
PBEsol0 | 0 | 0.00052198 | 0.0016896 | 0.0022872 | 0.020449 | 0.029939 | 0.0403 | 0.044224 | 0.10971 | 0.15258
PBE | 0 | 0.0024484 | 0.006491 | 0.008477 | 0.025408 | 0.04773 | 0.051812 | 0.086935 | 0.15485 | 0.23365
1nm
SrO surface

## Slide 63: Stable according to DFT
Chart: 
| 0.5 | 1.5 | 1.5 | 1.5 | -0.5 | 1.2692307692307692 | 1.1000000000000001 | 1.3888888888888888
100 | 1.3727 | 1.7778 | 1.7028 | 1.4621 | 1.292 | 1.2389 | 1.3625 | 1.3313
 | 1.192 | 1.1389 | 1.3621
 | 1.392 | 1.3389 | 1.5621
SrO
Ö2
2x2
c4x2
TiO2
Ö13
Ö5
3x3
TiO2 per 1x1
eV/1x1 cell, revTPSSh
D. M. Kienzle, A. E. Becerra-Toledo, and L. D. Marks, PRL. 106, 176102 (2011)
Acetic Acid
Oleic Acid

## Slide 64: Four examples
Connect TED, DFT, STM (and chemistry); the SrTiO3 (110) surface
What lies beyond order: glass-like tilings on SrTiO3, the Ö13xÖ13 (001) reconstruction
Surface Structure of Nanocuboid SrTiO3
Some additional complications: SrTiO3 (111), water and beyond

## Slide 65: Reality Checkpoint I
Are all your surfaces clean?
Are you really sure?
Really?

## Slide 66: Conundrum
2×1
Determined via transmission electron diffraction*
Supported by SXRD†
High surface energy‡
2×1
RT2
Lowest energy‡
But never observed!
(√2×√2)R45° (“RT2”)
Why??
Top View
Side View
* Erdman et al. Nature 419, 55 (2002)
‡ Warschkow et al., Surf.Sci. 573, 446 (2004)
† Herger et al. PRL 98, 076102 (2007)

## Slide 67: OH on SrTiO3 (100) (2x1)
67
Chart: Binding Energy (eV)

## Slide 68: 2×1: ½ML H2O Coverage
2x1Mol
2x1Diss
Top
View
Side
View

## Slide 69
Dry
½ ML
1 ML
“2Ti”
RT2
2×2
c(4×2)
(Top View)

## Slide 70: Energy
RT2 not lowest energy structure when surfaces are “wet”
Suggests: H2O opens kinetically favorable pathways to other structures
Becerra-Toledo, A.E., M.R. Castell, and L.D. Marks, Surface Science, 2012. 606(7-8), 762;
Becerra-Toledo, A.E., J.A. Enterkin, D.M. Kienzle, and L.D. Marks, Surface Science, 2012. 606(9-10), 791

## Slide 71: Reality Checkpoint II
The results shown are just the tip of the iceburg
There are many more kinetic/thermodynamic reconstructions

## Slide 72: More Ti-enriched surface
Ti dosage (ML)
Sr dosage (ML)
(6×1)
(5×1)
(4×1)
(2×4)
(6×4)
(n×1)
(m×4)
Z. Wang et al., Phys. Rev. B (2011)
(1×4)
(1×5)
(1×1)

## Slide 73: What do we know
SrTiO3 surfaces make semiconductors (and metals) look simple
  Simple 1x1 assumptions for SrTiO3 are inappropriate and bad science
  Why should other perovskites be simpler?
  Disordered (glass) structures possible
  Chemisorbed water can be present
  Extensive data already exists that growth depends upon initial reconstructions

## Slide 74
God made the bulk; the surface was invented by the devil
Wolfgang Pauli
Questions?