## Slide 1: Precession Diffraction: The Philospher’s Stone of Electron Crystallography?

## Slide 2: Focus
Many methods exist for obtaining diffraction information
  Selected Area
  Nanodiffraction and variants
  CBED
All are complicated to interpret
Reciprocal space is right, but intensities depend upon thickness, tilt etc

## Slide 3: What PED can do
We would like a method where not just the positions of the spots, but also the intensities could be used.
Not rigorously equivalent to simple kinematical diffraction, but has many similarities
  If the structure factor is large  Intensity is large
  Useful for fingerprinting structures
  Often does not need calculations to interpret

## Slide 4
History – Electron Precession (1993)
e-
e-


Advantages:

## Slide 5
Scan
De-scan
Specimen
Conventional Diffraction Pattern
Precession…
Precession Diffraction Pattern
(Ga,In)2SnO5 Intensities
412Å crystal thickness
Non-precessed
Precessed
(Diffracted amplitudes)

## Slide 6: Precession System
US patent application:
“A hollow-cone electron diffraction system”.
Application serial number 60/531,641, Dec 2004.

## Slide 7
Can be easily retrofitable to any TEM 100- 300 KV
precession is possible for any beam size 300 - 50 nm
Precession is possible for a parallel or convergent beam
precession eliminates false spots to ED pattern that belong to dynamical contributions
precession angle can vary continuously (0°-3°) to observe true crystallographic symmetry variation
Software ELD for easy quantification of ED intensities and automatic symmetry ( point, space group ) research
SPINNING STAR : UNIVERSAL INTERFASE FOR PRECESSION ELECTRON DIFFRACTION FOR ANY TEM ( 120 -200 -300 KV )
Easily interfaced to electron diffractometer for automatic 3D structure determination

## Slide 8: Examples:
Complicated Structures
  Hard to interpret SAED
  Simple to interpret PED
EDS
  Elemental ratio’s depend upon orientation in standard mode
  Weak to no dependence with PED

## Slide 9
APPLICATION : FIND TRUE CRYSTAL SYMMETRY
PRECESSION OFF
IDEAL KINEMATICAL (111)
UVAROVITE (111)
PRECESSION ON
Courtesy M.Gemmi
Univ of Milano

## Slide 10
APPLICATION : PERFECT CRYSTAL ORIENTATION
PRECESSION OFF
PRECESSION ON
Crystals –specially minerals -usually grow in platelet
or fiber shape and results dificult to orient perfectly in a particular zone axis; in this example olivine crystals are perfectly oriented after precession is on.
OLIVINE
Courtesy X.Zou, S.Hovmoller Univ Stockholm

## Slide 11: Carbide

## Slide 12: EDS, on zone (SrTiO3)
Repeat
Measurements

## Slide 13: Practical Use
Two commercial systems (one hardware, another software) are available
Not complicated, and could probably be written in scripting language
Alignment can be tricky – it always is
Not rocket science, to use

## Slide 14: Some Practical Issues
Bi-polar push-pull circuit (H9000)
Projector Spiral Distortions (60 mRad tilt)

## Slide 15
Block Diagram
‘Aberrations’
e-
e-



## Slide 16: Remember the optics
Sample
Objective Postfield
Objective Prefield
Better Diagram
Postfield Misaligned
Idealized Diagram
Descan
Scan

## Slide 17
Sample
Objective Postfield
Objective Prefield
Descan
Scan
Correct Diagram
Both Misaligned
Idealized Diagram
Remember the optics

## Slide 18: Alignment can be tricky

## Slide 19: Why?
Although PED has been around since 1992, and very actively used for ~10 years (mainly in Europe), there is no simple explanation (many have tried and failed)
Explanation is a bit rocket science

## Slide 20: Why?
What, if any generalizations can be made?
Role of Precession Angle
  Systematic Row Limit
Importance of integration
  Phase insensitivity
  Important for which reflections are used
  Fast Integration Options

## Slide 21: Ewald Sphere Construction
z
0
g
k
s
k+s
sz
Scan
De-scan
Specimen
(Diffracted amplitudes)

## Slide 22: Levels of theory
Precession integrates each beam over sz
Full dynamical theory
  All reciprocal lattice vectors are coupled and not seperable
Partial dynamical theory (2-beam)
  Consider each reciprocal lattice vector dynamically coupled to transmitted beam only
Kinematical theory
  Consider only role of sz assuming weak scattering
Bragg’s Law
  I = |F(g)|2

## Slide 23: Early Models
Iobs depends upon |F(g)|, g, f (precession angle) which we “correct” to the true result
Options:
0) No correction at all, I=|F(g)|2
1) Geometry only (Lorentz, by analogy to x-ray diffraction) corresponds to angular integration
2) Geometry plus multiplicative term for |F(g)|

## Slide 24: Bragg’s Law fails badly (Ga,In)2SnO5
3.2 Å; R=0.02
50 Å; R=0.19
100 Å; R=0.25
200 Å; R=0.49
400 Å*; R=0.78
800 Å; R=0.88

## Slide 25: Kinematical Lorentz Correction
I(g) =ò |F(g) sin(ptsz)/(psz) |2 dsz
sz taken appropriately over the Precession Circuit
t is crystal thickness (column approximation)
f is total precession angle
I(g) = |F(g)|2L(g,t,f)
K. Gjønnes, Ultramicroscopy, 1997.

## Slide 26: Kinematical Lorentz correction: Geometry information is insufficient
Need structure factors to apply the correction!
Fkin
Fcorr

## Slide 27: 2-Beam (Blackman) form
Limits:
  Ag small; Idyn(k) µ Ikin(k)
  Ag large; Idyn(k) µ ÖIkin(k) = |Fkin(k)|
But…
This assumes integration over all angles, which is not correct for precession (correct for powder diffraction)

## Slide 28: Blackman Form

## Slide 29: Blackman+Lorentz
Chart: Thickness
Alas, little better than kinematical
Comparison with full calculation, 24 mRad
Angstroms

## Slide 30: Two-Beam Form
I(g) = ò | F(g) sin(ptseffz)/(pseffz) |2 dsz
sz taken appropriately over the Precession Circuit
szeff = (sz2 + 1/xg2)1/2
Do the proper integration over sz (not rocket science)

## Slide 31: Two-Beam Integration: Ewald Sphere
Small (hkl)
Large (hkl)
Medium (hkl)
Chart: 

## Slide 32: 2-Beam Integration better
3.2 Å; R=0.02
50 Å; R=0.19
100 Å;R=0.24
200 Å; R=0.44
400 Å*; R=0.62
800 Å; R=0.67

## Slide 33: Some numbers
R-factors for 2-beam model
R-factors for kinematical model
See Sinkler, Own and Marks, Ultramic. 107 (2007)

## Slide 34: Fully Dynamical: Multislice
“Conventional” multislice (NUMIS code, on cvs)
Integrate over different incident directions 100-1000 tilts
f = cone semi-angle
  0 – 50 mrad typical
t = thickness
  ~20 – 50 nm typical
  Explore: 4 – 150 nm
g = reflection vector
  |g| = 0.25 – 1 Å-1 are structure-defining
2f
t

## Slide 35: Multislice Simulation
Multislice simulations carried out using 1000 discrete tilts (8 shown) incoherently summed to produce the precession pattern1
How to treat scattering?
Doyle-Turner (atomistic)
Full charge density string potential -- later
1 C.S. Own, W. Sinkler, L.D. Marks Acta Cryst A62 434 (2006)

## Slide 36: Multislice Simulation: works (of course)
R1 ~10% without refinement of anything

## Slide 37: Global error metric: R1
Chart: R-factor, (Ga,In)2SnO4
| 39.625 | 79.25 | 118.875 | 158.5 | 237.75 | 253.6 | 269.45 | 285.3 | 301.14999999999998 | 317 | 332.84999999999997 | 348.7 | 364.55 | 380.4 | 396.25 | 412.09999999999997 | 427.95 | 443.8 | 459.65 | 475.5 | 634 | 792.5 | 951 | 1109.5 | 1268 | 1426.5 | 1583.415
On Zone | 0.47077 | 0.65347 | 0.63033 | 0.67201 | 0.60542 | 0.63214 | 0.64381 | 0.63389 | 0.54718 | 0.43977 | 0.61079 | 0.55285 | 0.51559 | 0.53881 | 0.51094 | 0.50443 | 0.48817 | 0.49444 | 0.52762 | 0.49263 | 0.59105 | 0.55493 | 0.60871 | 0.56948 | 0.46227 | 0.63964 | 0.61101
Precession | 0.50002 | 0.45295 | 0.42427 | 0.37112 | 0.20385 | 0.18521 | 0.16834 | 0.14951 | 0.14278 | 0.13542 | 0.13092 | 0.12664 | 0.12534 | 0.1252 | 0.11845 | 0.11776 | 0.12321 | 0.13294 | 0.14626 | 0.16857 | 0.30777 | 0.28731 | 0.36987 | 0.40178 | 0.43422 | 0.45679 | 0.43393
Broad clear global minimum – atom positions fixed
R-factor = 11.8% (experiment matches simulated known structure)
  Compared to >30% from previous precession studies
Accurate thickness determination:
  Average t ~ 41nm (very thick crystal for studying this material)
(Own, Sinkler, & Marks, in preparation.)

## Slide 38: Quantitative Benchmark: Multislice Simulation
0mrad
10mrad
24mrad
75mrad
Experimental dataset
Error
g
thickness
(Own, Sinkler, & Marks, in preparation.)
Absolute Error = simulation(t) - kinematical
50mrad
Bragg’s Law

## Slide 39: Partial Conclusions
Separable corrections fail; doing nothing is normally better
Two-beam correction is not bad (not wonderful)
Only correct model is full dynamical one (alas)
N.B., Other models, e.g. channelling, so far fail badly – the “right” approximation has not been found

## Slide 40: Overview
What, if any generalizations can be made?
Role of Precession Angle
  Systematic Row Limit
Importance of integration
  Phase insensitivity
  Important for which reflections are used

## Slide 41: Role of Angle: Andalusite
Natural Mineral
  Al2SiO5
  Orthorhombic (Pnnm)
    a=7.7942
    b=7.8985
    c=5.559
  32 atoms/unit cell
Sample Prep
  Crushm Disperse on holey carbon film
  Random Orientation
2 C.W.Burnham, Z. Krystall. 115, 269-290, 1961

## Slide 42: Measured and Simulated Precession patterns
Bragg’s Law Simulation
Precession Off
6.5 mrad
13 mrad
18 mrad
24 mrad
32 mrad
Experimental
Multislice

## Slide 43: Decay of Forbidden Reflections
Decay with increasing precession angle is exponential
  The non-forbidden (002) reflections decays linearly
 | D(001) | D(003)
Experimental | 0.109 R2=0.991 | 0.145 R2=0.999
Simulated (102nm) | 0.112 R2=0.986 | 0.139 R2=0.963
Simulated 28-126 nm | 0.112±0.012 | 0.164±0.015
Rate of decay is relatively invariant of the crystal thickness
Slightly different from Jean-Paul’s & Paul’s – different case

## Slide 44: Quasi-systematic row
Projection of
Incident beam
Precession
Systematic Row
Forbidden, Allowed by Double Diffraction
On-Zone
Precessed

## Slide 45: Evidence: 2g allowed
Rows of reflections arrowed should be absent (Fhkl = 0)
Reflections still present along strong systematic rows
Known breakdown of Blackman model
Si [110]
Si [112]
e-
e-



## Slide 46: Phase and Averaging
For each of the incident condition generate 50 random phase sets {f} and calculate patterns:
Single settings at 0, 12, 24 and 36 mrad (along arbitrary tilt direction).
At fixed semi-angle (36 mrad) average over range of a as follows:
3 settings at intervals of 0.35º
5 settings at intervals of 0.35º
21 settings at intervals of 1º
For each g and thickness compute avg., stdev:
+
+
+
+
0 mrad
12
24
36
+
+
+
+

## Slide 47: Phase independence when averaged
single setting
3 settings, 0.35º interval
5 settings, 0.35º interval
21 settings, 1º interval (approaching precession)
Sinkler & Marks, 2009

## Slide 48: Why does it work?
If the experimental Patterson Map is similar to the Bragg’s Law Patterson Map, the structure is solvable – Doug Dorset
If the deviations from Bragg’s Law are statistical and “small enough” the structure is solvable – LDM

## Slide 49: Why is works - Intensity mapping
Iff Iobs(k1)>Iobs(k2) when Fkin(k1) > Fkin(k2)
  Structure should be invertible (symbolic logic, triplets, flipping…)
Chart: F kinematical
| 0 | 0.1 | 0.2 | 0.30000000000000004 | 0.4 | 0.5 | 0.6 | 0.7 | 0.79999999999999993 | 0.89999999999999991 | 0.99999999999999989 | 1.0999999999999999 | 1.2 | 1.3 | 1.4000000000000001 | 1.5000000000000002 | 1.6000000000000003
 | 0 | 0.099917 | 0.19933 | 0.29776 | 0.39471 | 0.48971 | 0.58232 | 0.67211 | 0.75868 | 0.84166 | 0.92074 | 0.9956 | 1.066 | 1.1318 | 1.1927 | 1.2487 | 1.2998
 | 0 | 0.17365 | 0.31041 | 0.37922 | 0.35974 | 0.24558 | 0.045278 | 0.21901 | 0.51502 | 0.80551 | 1.0541 | 1.231 | 1.3177 | 1.3101 | 1.2188 | 1.0676 | 0.89007

## Slide 50: Summary
PED is
  Approximately Invertable
  Pseudo Bragg’s Law
  Approximately 2-beam, but not great
  Properly Explained by Dynamical Theory
PED is not
  Pseudo-Kinematical (this is different!)
  Fully Understood by Dummies, yet

## Slide 51: Questions ?