## Slide 1: Where did that charge come from?
Karl Olson, Chris A. Mizzi, Alex Y. W. Lin and L. D. Marks
Northwestern University

## Slide 2: Tribology + Flexoelectricity = Triboelectricity
Mizzi, C.A., A.Y.W. Lin, and L.D. Marks, Does Flexoelectricity Drive Triboelectricity? Phys Rev Lett, 2019. 123(11): p. 116103 https://doi.org/10.1103/PhysRevLett.123.116103.
Mizzi, C.A. and L.D. Marks, The role of surfaces in flexoelectricity. Journal of Applied Physics, 2021. 129(22): p. 224102 https://doi.org/10.1063/5.0048920.
Mizzi, C.A. and L.D. Marks, When Flexoelectricity Drives Triboelectricity. Nano Lett, 2022, 22(10), 3939, https://doi.org/10.1021/acs.nanolett.2c00240.
Olson, K.P., C.A. Mizzi, and L.D. Marks, Band Bending and Ratcheting Explain Triboelectricity in a Flexoelectric Contact Diode. Nano Lett, 2022, 22(10), 3914 https://doi.org/10.1021/acs.nanolett.2c00107.

## Slide 3: Overview
Setting the Stage
  A few basics of Triboelectricity
  A few basics of Flexoelectricity
Tribology + Flexoelectricity = Triboelectricity ?

## Slide 4: Triboelectricity
First observed by Thales of Miletus around 585 BC after rubbing amber with fur
The source of the word electricity, which is derived from ēlektron, the Greek word for amber.

## Slide 5: Charge Transfer on sliding
Solid 1
Solid 2
Solid 1
Solid 2
+
+
+
+
-
-
-
-
-
-
-
-
+
+
+
+
Solid 1
Solid 2
+
+
+
+
-
-
-
-
-
-
-
-
+
+
+
+
Charged species may be electrons, ions, molecular fragments (evidence for all in different cases)

## Slide 6: Many Areas
Antistatic cloth
Weather
Safety
Power wearable electronics
Manufacturing
Dust Storms

## Slide 7: Current Models: Incomplete
Adapted from F. Galembeck et. al., RSC Advances 4(109) (2014) 64280-64298.
kb.staticworx.com/glossary/triboelectric-series/
Triboelectric Series

## Slide 8: Some of the issues
Charge transfer inhomogeneous
Curvature matters (first shown by Jameson in 1910, a school teacher from Glasgow, DOI: 10.1038/083189a0)
Tribocurrent scales as F1/3
Bipolar tribocharge (+/- during contact/pulloff)
Depends upon pre-strain of sample
Charge transfer can change sign with pressure
Occurs between different sized particles of the same material
Workfunction, dielectric constant, trap states matter

## Slide 9: You can’t beat Gibbs
Why does charge transfer occur?
The free energy change for charge separation must be negative
Why is rubbing required (Tribology)?
Mizzi, C.A., A.Y.W. Lin, and L.D. Marks, Does Flexoelectricity Drive Triboelectricity? Phys Rev Lett, 2019. 123(11): p. 116103 https://doi.org/10.1103/PhysRevLett.123.116103.
“In this house we obey the laws of thermodynamics”

## Slide 10: Friction is from plastic/elastic sliding of asperities
M. Falvo, Physics 267, http://www.physics.unc.edu/~falvo/phys267/index.html

## Slide 11: Can asperities lead to potentials?
M. Falvo, Physics 267, http://www.physics.unc.edu/~falvo/phys267/index.html

## Slide 12: Yes -- Flexoelectric Effect
Coupling between strain gradient and polarization:
Discovered in the 1960s, but largely unnoticed for decades in crystalline solids (very important in biology, e.g. cell membranes)
S. M. Kogan, Sov. Phys. Solid State 1964, 5, 2069–2070
E. V. Bursian, O. I. Zaikovskii, Sov. Phys. Solid State 1968, 10, 1121–1124

## Slide 13: Why?
d

## Slide 14: All Electromechanical Terms
Landau Expansion:
Gradient term adds an intrinsic 1/R dependence
Automatic “nano” dependence
Occurs in all insulators/semiconductors

## Slide 15: Established QM derivation
Moments of the change in charge density induced by the displacement of atom in direction
Changes in the positions of atom in direction caused by a strain gradient () and strain ()
Hong, J.W. and D. Vanderbilt, Physical Review B 2011. 84(18) 180101 https://doi.org/10.1103/PhysRevB.84.180101.
Zubko, P., G. Catalan, and A.K. Tagantsev, Annual Review of Materials Research, Vol 43, D.R. Clarke, Editor. 2013,. 387-421. https://doi.org/10.1146/annurev-matsci-071312-121634
Stengel, M.,. Physical Review B, 2016. 93(24) 245107 https://doi.org/10.1103/PhysRevB.93.245107.

## Slide 16: Flexocoupling voltage measurements
Classic 3-point bending experiment with conducting electrode and lock-in amplifier
e

## Slide 17: Flexocoupling voltages
Experimental data. Reasons for differences not yet clear
Mizzi, C. A.; Guo, B.; Marks, L. D. Physical Review Materials 2022, 6, (5), 055005.

## Slide 18: Measured flexocoupling voltage
Material | Space Group | Bending Direction | Flexocoupling Voltage (V)
MgO |  | [100] | 24±3
MgO |  | [111] | 62±7
SrTiO3 |  | [100] | 4.7±0.2
SrTiO3 |  | [110] | 3.1±0.5
KTaO3 |  | [100] | 2.3±0.5
TiO2 | P42/mnm | [100] | 3.1±1.0
DyScO3 | Pbnm | [110] | 42±2
YAlO3 | Pbnm | [101] | 26±1
LaAlO3 |  | [100] | 15±1
Material | Space Group | Bending Direction | Flexocoupling Voltage (V)
MgO |  | [100] | 24±3
MgO |  | [111] | 62±7
SrTiO3 |  | [100] | 4.7±0.2
SrTiO3 |  | [110] | 3.1±0.5
KTaO3 |  | [100] | 2.3±0.5
TiO2 | P42/mnm | [100] | 3.1±1.0
DyScO3 | Pbnm | [110] | 42±2
YAlO3 | Pbnm | [101] | 26±1
LaAlO3 |  | [100] | 15±1
Note: MgO anomalous
Mizzi, C. A.; Guo, B.; Marks, L. D. Physical Review Materials 2022, 6, (5), 055005.

## Slide 19: Typical polymer coefficients
1 B. Chu and D. R. Salem, Appl. Phys. Lett. 101, 103905 (2012).
2 J. Liu et al, Appl. Phys. Lett. 112, 232901 (2018).
3. M. Marvan and A. Havranek, Prog. Colloid Polym. Sci. 78, 33 (1988).
Reference | Material | ¦µ¦ (nC/m) | ¦f¦ (V)
1 | PVDF | 13 | 160
1 | Oriented PET | 9.9 | 289
1 | Polyethylene | 5.8 | 273
1 | Epoxy | 2.9 | 84
2 | P(VDF-TrFE) (70/30) | 3 | 31
2 | P(VDF-TrFE) (55/45) | 4.2 | 43
2 | PVDF | 3.5 | 10
3 | Jeffamine | ~ 0.1 | ~ 4.5
3 | Keltan | ~ 0.1 | ~ 4.5
3 | Natural Rubber | ~ 0.5 | ~ 20
Assume flexoelectric coefficient of 1 nC/m

## Slide 20: Growing Interest
U. K. Bhaskar, N. Banerjee, A. Abdollahi, Z. Wang, D. G. Schlom, G. Rijnders, G. Catalan, Nat. Nanotechnol. 2016, 11, 263–266.
Flexoelectric response in bone may stimulate healing
Flexoelectric actuators using SrTiO3 have comparable quality factors to best piezoelectric devices
F. Vasquez-Sancho, A. Abdollahi, D. Damjanovic, G. Catalan, Adv. Mater. 2018, 30, 1705316

## Slide 21: Back to Triboelectricity
Why does charge transfer occur?
The free energy change for charge separation must be negative
  Asperity contact/shear/bending leads to strain gradients
  Strain gradients lead to polarization (electric fields)
  Free energy of charge transfer negative
  Independent of whether this involves electrons, ions or charged molecular fragments.
Are the fields large enough to matter?

## Slide 22: Tribology + Flexoelectricity?
C. A. Mizzi, A. Y. W. Lin & L. D. Marks Phys Rev Lett. 2019;123(11):116103.

## Slide 23: Spherical Bicycle Approximation
Indentation
Pull-off
Pre-contact
Deformation fields
(Flexo)electric field

## Slide 24: Flexoelectric half-space
In a non-piezoelectric, dielectric material the dielectric displacement is given by:
Assumption #1: Isotropic material
x
z
Assumption #2: No surface charge

## Slide 25: Strain gradient terms
Units of 106 m-1

## Slide 26: Indentation Electric Fields
Tip Radius, (nm)
0.1-1 V/nm

## Slide 27: Pulloff case

## Slide 28: Spherical Bicycle Model
Does the bicycle work?
1-10 Volts with very conservative numbers for f (100V is not unreasonable)

## Slide 29: Tribocurrent scales as F1/3
J.V. Escobar, A. Chakravarty, S.J. Putterman. Diamond Relat. Mater. 36 (2013), 8-15.
S. Putterman

## Slide 30: Bipolar tribocharge transfer
T.A.L. Burgo, A. Erdemir. Angew. Chem. Int. Ed. 53 (2014), 12101-12105.
A. Erdimir

## Slide 31: Curvature dependence
Sign of charge/potential depends upon the curvature when using two pieces of the same material.
C. Xu et al., ACS Nano. 2019, 13, 2034-41.
Z. L. Wang

## Slide 32: Charge inhomogeneity
Charging is inhomogeneous
Local curvature differences (indentor versus indentee)
H.T. Baytekin, et al. Science 333 (2011), 308-312.
Persson, B. N. J. . EPL (Europhysics Letters) 2020, 129, (1), 10006.
B. Persson

## Slide 33: Strain Dependence
Two unstrained samples
One strained sample
A.E. Wang et al., Physical Review Materials 1(3) (2017) 035605.
Linear strain with a rough surface leads to local strain gradients
D. Lacks

## Slide 34: X-ray Emission from sellotape
C.G. Camara, et al. Nature 455 (2008), 1089-1092.
X-ray pulses during pulloff
What is f for sellotape?
Bending contribution?
S. Putterman

## Slide 35: Some of the issues
Charge transfer inhomogeneous
Curvature matters (first shown by Jameson in 1910, a school teacher from Glasgow, DOI: 10.1038/083189a0)
Tribocurrent scales as F1/3
Bipolar tribocharge (+/- during contact/pulloff)
Depends upon pre-strain of sample
Charge transfer can change sign with pressure
Occurs between different sized particles of the same material
Workfunction, dielectric constant, trap states matter

## Slide 36: Next Steps in Analysis
Charge transfer inhomogeneous
Curvature matters (first shown in 1908 by a school teacher from Glasgow)
Tribocurrent scales as F1/3
Bipolar tribocharge (+/- during contact/pulloff)
Depends upon pre-strain of sample
Charge transfer can change sign with pressure
Occurs between different sized particles of the same material
Workfunction, dielectric constant, trap states matter

## Slide 37: A lot now skipped…
Calculate the band bending
Include
Flexoelectric Strain gradient terms
Mean-inner potential
FEM (beyond Hertz solutions)
Mizzi, C.A. and L.D. Marks, When Flexoelectricity Drives Triboelectricity. Nano Lett, 2022, 22(10), 3939, https://doi.org/10.1021/acs.nanolett.2c00240

## Slide 38: Sphere on flat, same material
Band-Bending is asymmetric (Beyond Hertz)

## Slide 39: Charging with the same material
S.R. Waitukaitis, et al. Phys. Rev. Lett. 112 (2014), 218001.
Fused zirconium dioxide silicate particles of different sizes
H. Jaeger

## Slide 40: Sign change with Pressure
Sphere-on-flat contact band diagrams for a Si sphere (orange) on a SrTiO3 flat (blue). (a)-(c) show the conduction and valence band edges as a function of depth (normalized by the indenter radius R) at different contact pressures for a fixed radial distance of 0.6a from the contact point
Zener Tunnelling

## Slide 41: Reversal of charge transfer
Kelvin probe images obtained using different tips on SiOx substrates. a) CSG11 tip and b) NSG11 tip. The corresponding loaded forces are shown under each charge pattern. c) The loaded force dependence of surface potential when using NSG11 tips scanning over the SiOx surface.
Sun, H.; Chu, H.; Wang, J.; Ding, L.; Li, Y., Applied Physics Letters 2010, 96, (8), 083112.
Y. Li

## Slide 42: Quantitative Confirmation?
Charge transfer inhomogeneous
Curvature matters (first shown by Jameson in 1910, a school teacher from Glasgow, DOI: 10.1038/083189a0)
Tribocurrent scales as F1/3
Bipolar tribocharge (+/- during contact/pulloff)
Depends upon pre-strain of sample
Charge transfer can change sign with pressure
Occurs between different sized particles of the same material
Workfunction, dielectric constant, trap states matter

## Slide 43: AFM experiments
Olson, K.P., C.A. Mizzi, and L.D. Marks, Band Bending and Ratcheting Explain Triboelectricity in a Flexoelectric Contact Diode. Nano Lett, 2022, 22(10), 3914 https://doi.org/10.1021/acs.nanolett.2c00107.

## Slide 44: Flexoelectric Schottky Diode
Forward Current: Thermionic Emission
Reverse Current:
Thermally Assisted Tunnelling
Flexoelectric Band-Bending changes barrier

## Slide 45: CAFM Data
Forward
Fit for and
Reverse
Threshold bias where
Effective barrier

## Slide 46: Potential Terms
Mean Inner Potential
Flexoelectric Potential
Depletion Potential

## Slide 47: Calculate current
Radial section of band-bending for different forces
Saddle Point
Thermionic

## Slide 48: Comparison with experiment
Forward Reverse
Breakdown

## Slide 49: Charge Ratchetting

## Slide 50: Much still to be done
Beyond Hertzian & JKR – including shear terms
Bowden-Tabor ploughing contributions
Transfer layers, fracture contributions
Field induced chemical reactions (tribochemistry)
Plastic flexoelectric contributions (polar defects)
Gradient elasticity
Dynamics of charge transfer
Experiments & theory of above
…..
There is plenty of room at the bottom in triboelectricity

## Slide 51: Summary I
Triboelectricity
Tribology
+
=

## Slide 52: Summary II
Consistent with diverse old and new experimental observations, including
  Reversal of transfer with force
  Charging of identical materials
  Curvature and roughness dependence
  Temperature dependence
  Work function and dielectric constant dependence
  …
Contains no empirical, adjustable parameters
Consistent with other, known physics (band-bending etc)
All relevant terms can be measured/calculated (not so easy)

## Slide 53: Questions?
Research is to see what everybody else has seen, and to think what nobody else has thought Albert Szent-Györgi
Tribology + Flexoelectricity = Triboelectricity
Electric Collaborators Welcome: Laurence.Marks@gmail.com